## Slide 1: Manufacturing Engineering Technology in SI Units, 6th Edition Chapter 22: Cutting-Tool Materials and Cutting Fluids
Copyright © 2010 Pearson Education South Asia Pte Ltd
Manufacturing Processes (2), IE-352
Ahmed M El-Sherbeeny, PhD
Spring 2014
Notes: Presentation slide for courses, classes, lectures et al.

## Slide 2: Chapter Outline
Introduction
Cutting Tool Materials
  High-speed Steels
  Cast-cobalt Alloys
  Carbides
  Coated Tools
  Alumina-based Ceramics
  Cubic Boron Nitride
  Silicon-nitride-based Ceramics
  Diamond
  Whisker-reinforced Materials and Nanomaterials
Tool Costs and Reconditioning of Tools
Cutting Fluids
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 3: Introduction
Cutting tool is subjected to –as mentioned before– :
High temperatures,
High contact stresses
Rubbing along the tool–chip interface and along the machined surface
Cutting-tool material must possess:
Hot hardness (see right)
  compare ceramics vs. carbon steels
Toughness and impact strength
Thermal shock resistance
Wear resistance
Chemical stability and inertness (e.g. no adhesion)

## Slide 4: Introduction
Tool materials -see next 3 slides- may not have all of the desired properties for a particular machining operation:
  Hardness, strength: ensure good mechanical properties of workpiece material
  Impact strength: important for interrupted cuts (e.g. milling)
  Melting temperature: important for tool material due to high temp. generated in cutting zone
  Physical properties (e.g. thermal conductivity, coefficient of thermal expansion): ensure tool resistance to thermal fatigue, shock
  Compare (for example) in slide 6,
    High speed steels: high toughness, but low hot hardness
    Ceramics: high resistance to temp. & wear, but brittle and can chip
    Diamonds: hardest material, but most expensive

## Slide 5: Introduction

## Slide 6: Introduction

## Slide 7: Introduction

## Slide 8: Introduction
Tool Materials (also used for dies and molds in casting, forming, and shaping metallic and non-metallic materials):
High-speed steels
Cast-cobalt alloys
Carbides
Coated tools
Alumina-based ceramics
Cubic boron nitride
Silicon-nitride-based ceramics
Diamond
Whisker-reinforced materials and nanomaterials
Tools materials are discussed here in terms of:
  characteristics, applications, limitations, optimal performance

## Slide 9: High-speed Steels
High-speed steel (HSS) tools were developed to machine at higher speeds than was previously possible
  compared to carbon steels (low hot hardness ⇒low speeds)
Can be hardened to various depths, have good wear resistance and are inexpensive
Suitable for: high +ve rake angle tools, interrupted cuts, machines subject to vibration/chatter, complex tools
Biggest drawback: low cutting speed (V) vs carbide tools
Two basic types of HSS:
  molybdenum (M-series: 10% Mo; other alloys: Cr, V, W, Co): higher abrasion resistance than T-series, less distortion during heat treatment, less expensive ⇒ comprise 95% of HSS
  tungsten (T-series: 12-18% W ; other alloys: Cr, V, Co)

## Slide 10: High-speed Steels
High-speed steel tools are available in:
  wrought (rolled or forged)
  cast
  powder-metallurgy (sintered) forms
They can be treated to improve performance:
  Coating (discussed later)
  Surface treatment (to improve hardness, wear resistance)
  Steam treatment (reduce tendency of BUE formation)

## Slide 11: Cast-cobalt Alloys
Cast-cobalt alloys (mostly Co, also: Cr, W): have,
  high hardness
  good wear resistance
  maintain hardness at elevated temperatures (hot hardness)
Drawbacks
  not as tough as HSS
  sensitive to impact forces
  ⇒ less suitable than HSS for interrupted cutting operations
Applications: used as Stellite tools, used for
  Deep (large t0), roughing cuts (high f & V: twice larger > HSS)
  Removing large material (little concern for surface finish)
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 12: Carbides
AKA cemented/sintered carbides (since 1930’s)
Characteristics of carbides:
High hardness over a wide range of temperatures (&V )
  compared to HSS & Cast-Co alloys where only low V possible
High elastic modulus
High thermal conductivity
Low thermal expansion
Versatile
Cost-effective tool & die materials for many applications
2 groups used in machining (AKA uncoated carbides)
  Tungsten Carbide
  Titanium Carbide

## Slide 13: Carbides: Tungsten Carbide
Tungsten carbide (WC) consists of tungsten-carbide particles bonded together in a cobalt matrix (i.e. sintering)
  particle size is 1-5 μm
  particles are pressed and sintered into desired “insert” shapes
As Co content increases (typically: 6-16%),
  strength, hardness, and wear resistance of WC ↓
  yet toughness ↑ because of the higher toughness of Co
Applications:
  Cutting steels, cast irons, abrasive nonferrous materials
  Have largely replaced HSS due to better performance
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 14: Carbides: Titanium Carbide
Consists of a nickel–molybdenum matrix
wear resistance > tungsten carbide, but is not as tough
Applications:
  machining hard materials (steels and cast irons)
  cutting at speeds > those suitable for tungsten carbide
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 15: Carbides: Inserts
High-speed steel tools (i.e. traditional tools):
  1-piece; shaped for applications: drill bits, milling, gear cutters
  When cutting edge wears ⇒ tool must be replaced and sharpened, which is a time-consuming and inefficient process
Inserts: individual cutting tools with several cutting points
  e.g. Square insert: 8 cutting points (how?)
  Triangular insert: 6 cutting points
Typical carbide inserts with various shapes and chip-breaker features; note the complex chip breaking features on inserts

## Slide 16: Carbides: Inserts
Various locking mechanisms for inserts are used (below)
Clamping is the preferred method of securing an insert
  A particular edge is first used, then when edge is worn:
  insert is indexed (rotated in its holder) to make another cutting point available
clamping
wing lockpins
Inserts mounted with threadless lockpins (sidescrews)

## Slide 17: Carbides: Inserts
Carbide inserts: available in variety of shapes
  square, triangle, diamond, round (see below)
Strength of insert depends on its shape
  as included angle of cutting edge ↓⇒
  strength of the edge also ↓ and its chipping and breaking ↑

## Slide 18: Carbides: Inserts
Insert edges are usually
  honed, chamfered, produced with negative land (see below)
  this improves edge strength
  hone radius: about 0.025 mm

## Slide 19: Carbides: Inserts
Chip-breaker features on inserts (previous chapter)
Control chip flow during machining
Eliminate long –continuous– chips
Reduce vibration and heat generated
Selection of chip-breaker feature (slide 15) depends on
  f, t0, workpiece material, type of chip, roughing or finishing cut
Stiffness of the machine tool is important
  small f and V, and chatter are v. harmful to tool cutting edge
  light f : concentrate forces & temp. at tool edge ⇒ chipping
  small V ⇒ cold welding of chip to tool
  ⇒ cutting fluids needed in large, continuous amounts to minimize heating and cooling in interrupted cutting

## Slide 20: Carbides: Classification of Carbides
ISO (International Organization for Standardization):
  standards for carbide grades: classified using letters P, M, K
  difficult task due to various machining applications, materials
ANSI: other classification (C1-C8), depending on material

## Slide 21: Coated Tools
New alloys and engineered materials
  developed to have high strength and toughness (since 1960’s)
  problem: abrasive, chemically reactive with tool materials
  Difficulty in machining these materials  rise of coated tools
Coatings have unique properties:
Lower friction
Higher adhesion
Higher resistance to wear and cracking
Acting as a diffusion barrier
Higher hot hardness and impact resistance
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 22: Coated Tools
Coated tools:
  Tools lives up to 10X > uncoated tools
   allows higher V  reduced operation time & production costs
  machining time dropped by < 100 times since 1900 (see )
  Used now in 40-80% of all machining (esp. turning, milling, drilling)
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 23: Coated Tools: Coating Materials and Coating Methods
Common coating materials are:
Titanium nitride (TiN)
Titanium carbide (TiC)
Titanium carbonitride (TiCN)
Aluminum oxide (Al2O3)
Coatings usually have sizes: 2-15 m
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 24: Coated Tools: Coating Materials and Coating Methods
Techniques for applying coating on cutting tools & inserts:
Chemical-vapor deposition (CVD)
  used most with multiphase coating & ceramic tools (later)
Physical-vapor deposition (PVD)
  PVD-coated carbides with TiN coating 
    Higher cutting-edge strength
    Lower friction
    Lower tendency to form BUE
    Smoother and more uniform thickness (2-4 m)
    (note, how this covers all aspects of higher machinability in last chapter)
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 25: Coated Tools: Coating Materials and Coating Methods
Coatings for tools should have following characteristics:
High hardness: at high temp  resist wear
Chemical stability and inertness to workpiece  resist wear
Low thermal conductivity:  prevent rise in tool temp.
Compatibility and good bonding to substrate (i.e. tool material)  prevent flaking
Little or no porosity in coating  high strength and integrity
Additional enhancements to coating:
  Using substrate with high hardness, toughness
  Honing cutting edges to avoid peeling of coating at edges

## Slide 26: Coated Tools: Coating Materials and Coating Methods
Titanium-nitride Coatings
Have low friction coefficients, high hardness, resistance to high temperature, and good adhesion to substrate
Improve the life of high-speed steel tools and improve the lives of carbide tools, drill bits, and cutters
Perform well at higher cutting speeds and feeds
Flank wear « in uncoated tools (see right)
Flank surface can be reground after use without removing coating on rake face
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 27: Coated Tools: Coating Materials and Coating Methods
Titanium-carbide Coatings
Coatings have high flank-wear resistance in machining abrasive materials (used with WC inserts)
Ceramic Coatings
Ceramic serve well as coating material since
  chemically inert
  have low thermal conductivity,
  resist high temperature,
  resist flank and crater wear
Copyright © 2010 Pearson Education South Asia Pte Ltd
Notes: WC: Tungsten Carbide

## Slide 28: Coated Tools: Coating Materials and Coating Methods
Multiphase Coatings
Desirable properties of coatings can be combined & optimized with use of multiphase coatings
e.g. carbide tools with 3 layers
  TiC to bond with substrate (bottom)
  Al2O3 to bond well and be compatible with layer on top & bottom
  TiN to resist wear & have low thermal conductivity (top)
  usually used to machine cast iron or steel
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 29: Coated Tools: Coating Materials and Coating Methods
Alternating Multiphase Coatings
Size of each coating layer: 2-10 m
Note, thinner coating  grain size   hardness ↑
Inserts can have as many as 13 alternating layers
Copyright © 2010 Pearson Education South Asia Pte Ltd
TiN: low friction
Al2O3: therm. stability
TiCN: resists flank + crater wear

## Slide 30: Coated Tools: Miscellaneous Coating Materials
Polycrystalline diamond coating
  used especially with WC and SiN inserts
  used to machine abrasive, nonferrous metals (e.g. Al)
Titanium carbonitride (TiCN) and titanium-aluminum nitride (TiAlN): effective in cutting stainless steels
Chromium carbide (CrC) used to machine softer metals that adhere to cutting tool (e.g. Al, Cu, Ti)
More recent developments are nanolayer coatings and composite coatings
  Hardness almost as high as cBN
  Still in experimental phase
  Expected to have wide applications in machining
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 31: Coated Tools: Ion Implantation
Ions are introduced into the surface of the cutting tool, improving its surface properties
Process does not change the dimensions of tools
Nitrogen-ion implanted carbide tools have been used successfully on alloy steels and stainless steels
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 32: Alumina-based Ceramics
Ceramic tool materials
  consist of fine-grained and high-purity aluminum oxide
  additions of titanium carbide and zirconium oxide improve toughness and thermal shock resistance
  ceramic inserts used in high-speed cutting (e.g. turning)
Alumina-based ceramic tools
  high abrasion resistance and hot hardness (see below)
  more inert than HSS & carbides  less BUE (?)
   produce good surface finish with cast iron
  have low toughness  tend to chip prematurely
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 33: Alumina-based Ceramics
Cermets
Introduced in 1960’s
Consist of ceramic particles in a metallic matrix
e.g. cermet: 70% Al2O3 + 30% TiC
Have high chemical stability and resistance to BUE formation
But they are brittle, expensive and have limited usage
Performance is between ceramics and carbides
Application: high-speed finishing cuts
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 34: Cubic Boron Nitride
Cubic boron nitride (cBN): hardest material after diamond
  Carbide (substrate) provides shock resistance
  cBN layer provides v. high wear resistance & cutting-edge strength
At high temperatures, it is chemically inert to Fe & nickel
Its resistance to oxidation is high
Suitable for cutting hardened ferrous and high-temp alloys, and for high-speed machining
But: brittle, so machine must be stiff to resist vibrations
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 35: Silicon-nitride-based Ceramics
Silicon-nitride (SiN) based ceramic tool materials consist of silicon nitride with various additions of aluminum oxide, yttrium oxide and titanium carbide
Tools have:
  high toughness
  hot hardness
  good thermal-shock resistance
Due to chemical affinity to iron at elevated temperature, SiN-based tools are not suitable for machining steels
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 36: Diamond
Diamond: hardest of all known substances
Properties:
  low friction
  high wear resistance
  ability to maintain a sharp cutting edge
  result in good surface finish and high dimensional accuracy
  best used with soft nonferrous alloys
  also used with abrasive nonmetallic and metallic materials
Synthetic or industrial diamonds are used since natural diamond has flaws and performance can be unpredictable
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 37: Diamond
As diamond is brittle, tool shape and sharpness are important
  low rake angle must be used to provide strong cutting edge
  proper mounting should be used for optimum tool life
  best used with light, uninterrupted finishing cuts
  tool must be resharpened as soon as it becomes dull (to minimize fracture
Copyright © 2010 Pearson Education South Asia Pte Ltd
top row: Inserts with polycrystalline cBN tips
bottom row: Solid polycrystalline cBN inserts
Note: these are similar to diamond tools

## Slide 38: Whisker-reinforced Materials and Nanomaterials
Continuous effort to improve tool performance, increase wear resistance, and enhance properties:
High fracture toughness
Resistance to thermal shock
Cutting-edge strength
Creep resistance
Hot hardness
Whiskers: used for reinforcing fibers in composite tools
  e.g. Si-carbide whiskers: 5-100 m long, diameter: 0.1-1 m
Nanomaterials: also becoming important in tools
  e.g. carbides, ceramics; applied as thin coating
  Increase tool life without coolant (i.e. dry machining)

## Slide 39: Tool Costs and Reconditioning of Tools
Tool costs depend on: tool material, size, shape, chip-breaker features and quality; e.g. (12.5-mm insert):
  uncoated carbide: $5-10 (cheapest)
  diamond-tipped: $90-125 (most expensive)
Cost of individual insert is relatively insignificant
  tooling comprises only 2-4% of all machining costs
  reason: single tool can be indexed and recycled
  e.g. square insert with 1 edge lasting 30-60 min will last: ?*
Cutting tools can be reconditioned by resharpening
  carried out manually, or cutter grinders, or comp.-controlled
Reconditioning of coated tools also done by recoating
  must make sure dimensions are same as original tool
Notes: See slide 60 of previous chapter: 30-60 min for carbide tools
Square insert will last: ~ 45 min * 8 edges = 360 min
i.e. ~ 6 hours before replacement

## Slide 40: Cutting Fluids
Cutting fluids used to:
Reduce friction & wear ( improve tool life, surface finish)
Cool the cutting zone ( improve tool life,  temperature)
Reduce forces and energy consumption
Flush chips from cutting zone (important in drilling)
Protect machined surface from environmental corrosion
Cutting fluid used as (depending on machining operation):
  coolant, or lubricant, or both
  e.g. water: excellent coolant (i.e. temp ); but not effective lubricant (i.e. no  in friction); may also cause oxidation (rust)
Effectiveness of cutting fluids depends on:
  machining operation, tool & workpiece materials, cutting speed

## Slide 41: Cutting Fluids
Cutting-fluid Action
Cutting fluids move to tool-chip interface by
  Seeping (i.e. slow penetration) from sides of the chip
  capillary action of the “interlocking network of surface asperities” (i.e. unevenness) in the interface
Cutting fluids should thus have
  Small molecular size (for small capillary network)
  Appropriate “wetting” (high surface tension)
  e.g. using emulsions, low-weight oils suspended in water
Discontinuous cutting operations:
  have easier mechanisms for lubricant application
  but the tools are more susceptible to thermal shock
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 42: Cutting Fluids
EXAMPLE 22.2
Effects of Cutting Fluids on Machining
A machining operation is being carried out with a cutting fluid that is an effective lubricant. What will be the changes in the mechanics of the cutting operation if the fluid is shut off?
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 43: Cutting Fluids
Solution
Effects of Cutting Fluids on Machining
Chain of events taking place after the fluid is shut off:
Friction at the tool–chip interface will increase
The shear angle will decrease in accordance
The shear strain will increase
The chip will become thicker
A built-up edge is likely to form
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 44: Cutting Fluids
Solution
Effects of Cutting Fluids on Machining
As a result of these changes:
The shear energy in the primary zone will increase
The frictional energy in the secondary zone will increase
The total energy will increase
The temperature in the cutting zone will rise
Surface finish will deteriorate and dimensional tolerances may be difficult to maintain
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 45: Cutting Fluids
Types of Cutting Fluids (4 general types)
Oils (AKA straight oils)
  mineral, animal, vegetable, compounded, and synthetic oils
  used for: low-speed operations (i.e. no high ↑ in temperature)
Emulsions (AKA soluble oils)
  mixture of oil and water and additives
  used for: high-speed operations (i.e. high ↑ in temperature)
  water: acts as coolant; oils: reduces oxidation caused by water
Semisynthetics
  chemical emulsions + little water-diluted mineral oil + additives
Synthetics
  chemicals with additives, water-diluted, with no oil

## Slide 46: Cutting Fluids
Methods of Cutting-fluid Application
4 basic methods
Flooding
  Most common method (see next slide)
  Typical rate: 10 L/min (single-point tools, as in turning) to 225 L/min (multiple point cutters, as in milling)
  Chips flushed with 700-14,000 kPa pressures
Mist
  Similar to spraying with aerosol can
  Allows better view of machined workpiece (compared to flooding)
  But has lower cooling capability
  Also: venting needed to prevent inhalation of particles

## Slide 47: Cutting Fluids
Proper Methods of Applying Flooding (see below)
turning
milling
thread grinding
drilling

## Slide 48: Cutting Fluids
Cont. Methods of Cutting-fluid Application
High-pressure systems
  used to increase rate of heat removal from cutting zone
  nozzles: direct cutting fluid powerfully into relief (flank) face
  pressure used: 5.5-35 MPa
  may be used as chip-breaker (e.g. long, continuous chips)
Through the cutting tool system
  used when difficult to apply cutting fluid into the cutting zone
  narrow passage in cutting tool and tool holder
  used to supply cutting fluid under high pressure

## Slide 49: Cutting Fluids
Effects of Cutting Fluids
Selection of a cutting fluid is based on:
Workpiece material and machine tools
  Cutting fluids may react with machine tool components
  Thus, must clean machined parts from cutting fluids residue
Biological considerations
  Machine-tool operator is in close proximity to cutting fluids
  Thus, health effects is a primary concern
  Mist, fumes, smoke, cutting fluid odors  skin reactions, respiratory problems
  Progress made in ensuring the safe use of cutting fluids (e.g. by using dry or near-dry machining)

## Slide 50: Cutting Fluids
Cont. Effects of Cutting Fluids
Selection of a cutting fluid is based on:
Environment
  Cutting fluids may change –chemically– over time & repeated use
  Due to: environmental effects or contamination (e.g. metal chips)
  Result: development of microbes (especially in presence of water)  environmental hazard, decreased cutting fluid effectiveness
  Recycling involves treatment of fluids with additives, agents, biocides, deodorizers and water treatment
  Disposal must abide by local laws

## Slide 51: Cutting Fluids: Near-dry and Dry Machining
Trend since mid-1990’s to reduce cutting fluid usage
Thus, rise of near-dry machining; advantages:
  reducing health, environmental hazards of cutting fluids
  reducing cost of maintenance, recycling, disposing of CF’s
  improving surface quality
Near-dry cutting/machining (NDM)
  application of fine mist of air–fluid mixture containing very small amount of cutting fluid (« then used in flooding)
  also called minimum-quantity lubrication (MQL)
Dry machining
  effective for turning, milling on steels, steel alloys, cast irons
  here chips flushed from cutting zone by pressurized air
  i.e. air serves limited cooling & flushing, but no lubrication

## Slide 52: Cutting Fluids: Near-dry and Dry Machining
Cryogenic Machining
Using gases like nitrogen or carbon dioxide as a coolant
Small-diam. nozzle injects liquid N2 to cutting zone @ -200°C
Tool life & hardness maintained  higher cutting speeds
Also: chips are more brittle
Machinability is, thus, generally increased
Also, N2 evaporates; i.e. no adverse environmental effect
Copyright © 2010 Pearson Education South Asia Pte Ltd