## Slide 1: Manufacturing Engineering Technology in SI Units, 6th Edition Chapter 23: Machining Processes: Hole Making – Part B (Drilling)
Manufacturing Processes (2), IE-352
Ahmed M El-Sherbeeny, PhD
Spring 2017

## Slide 2: Drilling, Drills, and Drilling Machines
Most products have many holes in them
  e.g. for rivets on plane wings
  e.g. for bolts in engine blocks
Holes used for:
  assembly with fasteners (e.g. screws, bolts, rivets)
  design purposes (e.g. weight reduction, ventilation)
  appearance
Hole making:
  Among most important operations in manufacturing
  Drilling is major, common hole-making process
  Cost is among highest machining costs in car engine prodon
Notes: Rivets: threadless nails; Bolts: threaded nails; screws: small threaded nails

## Slide 3: Drilling, Drills, and Drilling Machines: Drills
Drill properties:
  Have high length-to-diameter ratios (see next slide)
  Thus, capable of producing deep holes
  Caution: drills are flexible  should be used with care
    to drill holes accurately
    and to prevent breakage
Drilling Marks:
  Drills leave burr* on bottom surface upon breakthrough
     requires deburring operations
  Rotary motion of drilling
     holes with “circumferential marks” on walls
Notes: * Burr: a rough area on a piece of metal that is left after the metal is cut

## Slide 4: Drilling, Drills, and Drilling Machines: Drills
2 common types of drills
a) margins: provide bearing surface for drill against walls of hole as it penetrates workpiece
b) have good centering ability, chips break easily  suitable for deep holes
(AKA: standard-point twist drill)
Notes: Bearing surface: i.e. support surface

## Slide 5: Drilling, Drills, and Drilling Machines: Drills
Drill oversize:
Oversize: fact that of hole > drill (slightly)
This is visible: easy to remove drill after making hole
Oversize depends on:
  Quality of drill
  Equipment
  Expansion of metallic/non-metallic material due to drilling heat
In the end: possible that final hole < drill
To improve S.F. and dim. acc.:
  Perform reaming/honing* on drilled holes
Capabilities of drilling/boring: shown on next slide
Notes: * Honing: abrasive machining process that produces a precision surface on a metal workpiece by scrubbing an abrasive stone against it

## Slide 6: Drilling, Drills, and Drilling Machines: Drills
Note, depth/diameter is a ratio (i.e. unitless)
  e.g. for twist drill:
  typical depth @

## Slide 7: Drilling, Drills, and Drilling Machines: Drills
Twist Drill
Most common drill: conventional standard-point twist drill
Geometry of drill point:
  normal rake angle and of cutting edge vary with distance from center of drill
Main features of twist drill (typical angles):
Point angle ()
Lip-relief angle ()
Chisel-edge angle ()
Helix angle ()

## Slide 8: Drilling, Drills, and Drilling Machines: Drills
Cont. Twist Drill
Grooves in drills:
  Spiral grooves run along length of drill
  Chips: guided through grooves, upward
  Grooves: also allow cutting fluid to reach cutting edges
  Some drills have internal longitudinal holes for cutting fluids (a)  lubrication, cooling, flushing chips
  Drills have chip-breaker feature ground along cutting edges
Drill angles (chosen carefully):
  Produce accurate holes
  Minimize drilling forces and torque
  Increase drill life
  Small change in angles  great change in performance*
Notes: * e.g. too small lip relief angle  increased thrust force  increased heat  increased wear, while too large angle  chipping/breaking of cutting edge

## Slide 9: Drilling, Drills, and Drilling Machines: Drills
Other Types of Drills
Step drill:
  Holes with 2 ’s
Core drill:
  Enlarge existing hole
Counter boring/countersinking:
  Make depressions on surfaces to accommodate heads of screws, bolts below workpiece surface
Center drill:
  Short; produce hole at end of piece of stock
Spot drill:
  Spots (i.e. starts) hole at desired location on a surface

## Slide 10: Drilling, Drills, and Drilling Machines: Drills
Other Types of Drills
Spade drills (a):
  Removable bits
  Large holes
  Deep holes
  Advantages: high stiffness, ease of grinding edges, low cost
Straight-flute drill (b):
  Similar to spade drill
Solid carbide (c), carbide-tipped drills* (d) for drilling:
  Hard materials (e.g. cast irons)
  High-temp. metals
  Abrasive (e.g. concrete) and composite materials (e.g. glass)
(indexable)
Notes: * Note that, unlike in c), the body of the carbide-tipped drills (d) are made of steel (low-alloy) and carbide tip is brazed

## Slide 11: Drilling, Drills, and Drilling Machines: Drills
Gun Drilling
Name origin “gun”
  Drilling gun barrels
Features:
  Drilling deep holes
  Requires a special drill
  Hole depth-to- ratio:
  balanced by bearing pads on inside surface
   gun drill: self-centering (important for drilling deep holes)
Gun trepanning:
  Uses cutting tool similar to gun drill
  Tool has a central hole
Gun drill
Gun drilling operation
Notes: : thrust force (radial force that tends to push drill sideways)
𝐹_𝑡: thrust force (radial force that tends to push drill sideways)

## Slide 12: Drilling, Drills, and Drilling Machines: Drills
Cont. Gun Drilling
Cutting fluid
  Forced under high pressure through passage in drill body (fig a)
  Cooling and lubrication effect
  Also: flushes out chips that could be trapped in deep holes
   chips don’t interfere with drilling operation
   no need to retract tool to clear chips (i.e. unlike twist drills)

## Slide 13: Drilling, Drills, and Drilling Machines: Drills
Trepanning
Name origin:
  “Trypanon” (Greek) i.e. boring a hole
Cutting tool produces a hole:
  By removing a disk-shaped piece (core) from flat plates
  Without changing all material to chips (i.e. unlike drilling)
Can make disks:
  Up to in diameter
  From flat sheets, plates, structural members (e.g. I-beams)
Carried out:
  On lathes, drill presses, or other machine tools
  Using single-point or multipoint tools (fig. b)

## Slide 14: Drilling, Drills, and Drilling Machines: Drills
Cont. Trepanning
a) Trepanning tool
b) Trepanning with drill-mounted single cutter

## Slide 15: Drilling, Drills, and Drilling Machines: Material-removal Rate in Drilling
Material-removal rate (MRR) in drilling:
  Volume of material removed per unit time*
Drill diameter:
C.S.A. of drilled hole:
Velocity of drill ( to workpiece):
  , feed: dist. drill penetrates/unit rev., i.e.
  : rotational speed

  Check dimensions: (which are units of volume / unit time)
Notes: * note, MRR means the same in all machining operations (i.e. vol. of material removed per unit time)

## Slide 16: Drilling, Drills, and Drilling Machines: Thrust Force and Torque
Thrust force ()
  Acts perpendicular to hole axis (i.e. radially or sideways)
  Excessive 
    Drill: bends or breaks
    Workpiece: distorted (esp. if it does not have sufficient stiffness*)
    or Workpiece: slips into workholding fixture
depends on:
  Strength of the workpiece material
  Feed
  Rotational speed
  Drill diameter
  Drill geometry
  Cutting fluid
Notes: * e.g. this may happen with thin sheet-metal structures

## Slide 17: Drilling, Drills, and Drilling Machines: Thrust Force and Torque
Finding :
  Accurate calculation is difficult
  Range:
    few for small drills
    to for high-strength materials with large drills
  Experimental data: helps in using drills

## Slide 18: Drilling, Drills, and Drilling Machines: Thrust Force and Torque
Torque
Knowledge of torque () in drilling:
  Essential for estimating the power requirement
  But difficult to calculate (due to many factors involved)
can be estimated from data tables:
  e.g. table showing sp. power for different materials (Table 21.2)
  Note, power dissipated in drilling = torque * rotational speed
  i.e.
  Remember,
  
  Note, for proper units: must be expressed as:
    : rotational speed from to **
Notes: * note, T can be as high as 4,000 Nm ** note; 1 rev. = , and 1 min. = 60 s
* note, T can be as high as 4,000 N∙m ** note; 1 rev. = 2𝜋 𝑟𝑎𝑑, and 1 min. = 60 s

## Slide 19: Drilling, Drills, and Drilling Machines: Thrust Force and Torque
EXAMPLE 23.4
Material-removal Rate and Torque in Drilling
A hole is being drilled in a block of magnesium alloy with a drill bit at a feed of and with the spindle running at . Calculate the material-removal rate and the torque on the drill.

## Slide 20: Drilling, Drills, and Drilling Machines: Thrust Force and Torque
Solution
Material-removal Rate and Torque in Drilling
The material-removal rate is
The power required is
The torque is
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 21: Drilling, Drills, and Drilling Machines: Drill Materials and Sizes
Drill materials:
  Usually made from
  Also solid carbides or with carbide tips
Drills commonly coated with:
  or * for increased wear resistance
Polycrystalline-diamond-coated drills:
  Used to make fastener holes
  Used with fiber-reinforced plastics
  Have high wear resistance
  1000’s of holes can be drilled with little damage to drill material
Notes: * remember: TiN and TiCN: titanium nitride and titanium carbonitride (which are commonly used as coating materials)

## Slide 22: Drilling, Drills, and Drilling Machines: Drill Materials and Sizes
Standard twist-drill sizes consist of following series:
Numerical
  No. ( ) to No. ()
Letter
  A ( ) to Z ()
Fractional
  Straight shank: from (in increments) to (in increments)*
  Taper shank: (in ) to (in )
Millimeter
  From () in
Notes: * For larger drills, larger increments are used; note:
* For larger drills, larger increments are used; note: 1 𝑖𝑛. = 25.4 𝑚𝑚

## Slide 23: Drilling, Drills, and Drilling Machines: Drilling Practice
Drill chucks:
  Used to hold drills (and similar hole-making tools)
  Tightened with/without keys
  Special chucks
    Have quick change features
    Do not require stopping the spindle
    Available for use in production machinery
Lateral deflection of drill:
  Drills do not have a centering action
   tend to “walk” on workpiece surface at start of operation
  Problem severe with small-D long drills, may lead to failure

## Slide 24: Drilling, Drills, and Drilling Machines: Drilling Practice
Avoiding lateral deflection of drill (at start of drill):
  Guide drill using fixtures
  Use center drill to make small starting hole before drilling
    Usually @ point angle
  Grind drill point to an S shape (important with CNC machines)
    This has a self-centering characteristic
     no need for center-drilling
    Produces accurate holes with improved drill life
  Use centering punch  produces initial impression
  Add dimples (or other features) in cast or forged blank
Copyright © 2010 Pearson Education South Asia Pte Ltd

## Slide 25: Drilling, Drills, and Drilling Machines: Drilling Practice
Drilling Recommendations
Speed:
  Recommended ranges for and shown in table (next slide)
  Speed here is surface speed, , of drill at its periphery
  Example: drill, rotating at *, has a surface speed of:
  Note how surface speed () is different than drill velocity ()
  Drilling holes (in diameter):
    can be up to (depending on workpiece material)
Notes: * Q: Can you guess what material(s) this example can be applicable to; A: titanium alloys or stainless steels

## Slide 26: Drilling, Drills, and Drilling Machines: Drilling Practice
Drilling Recommendations

## Slide 27: Drilling, Drills, and Drilling Machines: Drilling Practice
Drilling Recommendations
Feed:
  Feed in drilling: dist. drill travels into workpiece per revolution
  Recommendation: for most workpiece materials: drills with should have
  Example: A drill rotating at , has linear speed of:

## Slide 28: Drilling, Drills, and Drilling Machines: Drilling Practice
Drilling Recommendations
Chip removal during drilling:
  Can be difficult
  Especially: deep holes in soft and ductile workpiece materials
  To avoid this:
    Retract drill periodically (“pecking”), then:
    Removing chips accumulated along drill flutes
    Otherwise: drill may break due to high , or “walk-off” location and produce mis-shaped hole
  Table: shows guide to general problems in drilling operations

## Slide 29: Drilling, Drills, and Drilling Machines: Drilling Practice
Drilling Recommendations

## Slide 30: Drilling, Drills, and Drilling Machines: Drilling Practice
Drill Reconditioning
Drills reconditioned by grinding, either:
  Manually (i.e. by hand), or
  With special fixtures
Reconditioning: especially important with CNC machines
Hand grinding:
  Difficult
  Requires considerable skill to produce symmetric cutting edges
Grinding on fixtures:
  Accurate
  Done on special computer controlled grinders
Coated drills can be recoated

## Slide 31: Drilling, Drills, and Drilling Machines: Drilling Practice
Measuring Drill Life
Drill life measured by no. of holes drilled:
  Before they become dull, and
  Need to be re-worked or replaced
Determining drill life experimentally:
  Clamping material on dynamometer/force transducer
  Drilling number of holes
  Recording or during each operation
  After certain no. of holes: & since tool becomes dull
  Drill life here is: no. of holes drilled until this transition begins
Other techniques to measure drill life:
  Monitoring vibrations and acoustic emissions (Ch. 21: tool life)

## Slide 32: Drilling, Drills, and Drilling Machines: Drilling Machines
Drilling machines
  Used for drilling holes, tapping, reaming and small-diameter boring operations
  Most common machine: drill press (fig. a)
Drilling process:
  Workpiece is placed on adjustable table by:
    Clamping directly into slots and holes in the table, or using:
    Vise* (: swivel vise), which’s then clamped to table
  Drill is lowered:
    Manually (requires skill in judging appropriate ), or:
    Using handwheel, or:
    By power feed at preset rates
Notes: * vise: tool for holding a workpiece with two jaws usually with screws

## Slide 33: Drilling, Drills, and Drilling Machines: Drilling Machines
Schematic: components of vertical drill
Radial drilling machine

## Slide 34: Drilling, Drills, and Drilling Machines: Drilling Machines
Drill presses:
  Designated by largest workpiece accommodated on table
  Typical range
Adjusting spindle speed
  Necessary to maintain proper cutting speed at drill cutting edge
  Allows using different drill sizes
Types of drilling machines (traditional machines)
  Simple: bench type drills, used to drill small- holes
  Large: radial drills (fig. b), used for large workpieces
  Universal drilling machines: drill head can be swiveled to drill holes at an angle

## Slide 35: Drilling, Drills, and Drilling Machines: Drilling Machines
Cont. Types of drilling machines (developments):
  Numerically controlled three-axis drilling machines (fig.):
    Operations performed automatically & in desired sequence using turret
    Turret holds different tooling tools
  Gang drilling:
    Drilling machines with multiple spindles*
    Used for high-production-rate operations
    Capable of drilling 50 holes in 1 cycle (different sizes, depths, locations)
    Also used for reaming, counterboring operations
  Numerical-control turret drilling machines
    Replacing machine tools and gang-drilling machines
  Special drilling machines
    e.g. produce holes in continuous hinges (e.g. piano hinges)
    Horizontal and produce holes up to long segments per cycle
Notes: * note, all previously mentioned involve only 1 spindle

## Slide 36: Drilling, Drills, and Drilling Machines: Drilling Machines
3-axis NC drilling machine; turret holds as many as 8 different tools (e.g. drills, taps, reamers)
Notes: * Q: why is it called a 3-axis drilling machine? A: look at the 3, 2-sided arrows and you will know

## Slide 37: Drilling, Drills, and Drilling Machines: Drilling Machines
Workholding devices:
  Ensure workpiece is located properly
  Keep workpiece from slipping or rotating during drilling
  Available in various designs
  Important features:
    3-point locating (for accuracy)
    3-D workholding for secure fixtures
Notes: * note, all previously mentioned involve only 1 spindle

## Slide 38: Drilling, Drills, and Drilling Machines: Design Considerations for Drilling
Basic design guidelines for drilling:
  Designs should allow holes to be drilled
    On flat surfaces and  to drill motion
    Otherwise: drills deflect and hole will not be located properly
  Interrupted hole surfaces should be avoided
    This ensures: dim. acc., longer drill life, avoids vibrations
  Hole bottoms should match standard drill-point angles
  Through holes are preferred over blind holes
  Dimples should be provided:
    When pre-existing holes not possible, to reduce drill “walk-off”
  Parts should be designed to drill with minimum of fixturing
  Blind holes: drill deeper than subsequent reaming/tapping