## Slide 1
8. SOIL COMPACTION

## Slide 2
INTRODUCTION
In Geotechnical engineering practice, the soils at a given site are often less than desirable for the intended purpose. They may be:
Week (strength)
Highly compressible
Have a high permeability
Solution
Relocate the project
Articulate design for structure members
Stabilize or improve the properties of the soil
The third alternative may be the most economical alternative. There are different techniques for improvement of soils (This subject is covered in details in CE 586 “Improvement of Geotechnical Materials”).
We will consider in this course only compaction.

## Slide 3
Compaction is also very important when soil is used as an engineering material, that is the structure itself is made of soil.
Ex.
Earth dams
Highways
Airfields
etc.
Compaction is the densification of soils by the application of mechanical energy.
Definition
The degree of compaction is measured in terms of its dry unit weight.

## Slide 4
Air
Water
Solid
Air
Water
Solid
Compaction
You remember well graded

## Slide 5
General Principle
The degree of compaction of soil is measured by its dry unit weight. When water is added during compaction it acts as a softening agent on the soil particles.
Soil Solid
Soil Solid
water
Optimum moisture content (OMC) is the water content at which the maximum dry unit weight is attained.
When the moisture content is gradually increased, the weight of the soil solids in a unit volume gradually increases.
d(max)

## Slide 6
Types of Compaction Methods in the Laboratory
Impact or dynamic (The most common type)
Kneading
Static
Standard Proctor test
Modified Proctor test
The laboratory test generally used to obtain the maximum dry unit weight of compaction and the optimum moisture content is called the Proctor compaction test.
There are two methods or tests:
It is named after R. R. Proctor (engineer in LA). He established that compaction is a function of four variables:
Dry density,
Moisture Content
Compactive Effort
Soil Type

## Slide 7
Standard Proctor Test
Mold 1/30 ft3 in volume
3 layers
25 blows
5.5 lb hammer
12 inch drop
Mold
Hammer
E =
The procedure for the standard Proctor test is elaborated in ASTM Test Designation D-698 (ASTM, 2007) and AASHTO Test Designation T-99 (AASHTO, 1982).

## Slide 9
Process of Compaction
Several samples are mixed at different water contents
W = Weight of compacted soil in the mold
Vmold = Volume of the mold = (1/30 ft3)
Compact according to the compaction test (standard or modified).
For each test find the moisture content of the compacted soil.
The dry unit weight is given by
From the plot, find OMC and
Plot vs. w

## Slide 10
Remarks
Each data point on the curve represent a single compaction test.
Four or five tests are required
The curve is unique for:
- A given soil type
- Method of compaction
- (constant) compactive effort
d(max) is only a maximum for a specific compactive effort and method of compaction. This does not necessarily reflect the maximum dry unit weight that can be obtained in the field.
Typical OMC are between 10% and 20%. Outside maximum range 5% to 40%.
Increasing the compactive effort tends to increase the maximum dry density, as expected, but also decrease the OMC. (This is why the curve never be to the right of zero curve).

## Slide 11
For clay soils d(max) tends to decrease as plasticity increases.
The approximation to field is not exact because the lab. test is a dynamic impact type, whereas field compaction is essentially a kneading-type compaction.
In practice less amount of water is used but higher compactive effort or vise versa.
Remarks (Cont.)
For other types of compaction (i.e. kneading and static) the calculation of compactive effort is not a simple matter.
In the field, compactive effort is the number of passes or “coverage” of the roller of a certain type and weight on a given volume of soil.

## Slide 12
Theoretical
The maximum is obtained when no air in the voids (i.e. s =100%)
Where zav = zero air void unit weight.
The relationship between zav and w can be obtained as shown in the figure across.
Compaction curve is always to the left of the zero-air-void curve.
No matter how much water is added, the soil never becomes completely saturated by compaction.
Impossible zone

## Slide 13
Factors affecting Compaction
Besides moisture content, other important factors that affect compaction are: 1) Soil type; 2) Compaction effort.
1. Effect of Soil Type
GSD
Shape of the soil grains
Gs
Amount of clay minerals
Type of clay minerals
Fine grain soil needs more water to reach optimum.

## Slide 14
Effect of Soil type and gradation (cont.)
Fine grain soil needs more water to reach optimum.

## Slide 15
Gs is constant, therefore increasing maximum dry unit weight is associated with decreasing optimum moisture contents.
Do not use typical values for design as soil is highly variable.
Effect of Soil type and gradation (cont.)
Typical Values
(kN/m3)
OMC (%)
Well graded sand SW
22
7
Sandy clay SC
19
12
Poorly graded sand SP
18
15
Low plasticity clay CL
18
15
Non plastic silt ML
17
17
High plasticity clay CH
15
25

## Slide 16
The bell-shaped compaction curve is typical for most clayey soils.
Some curves have more than one peak others have no peak.
Compaction Curves Encountered in Soils

## Slide 17
2. Effect of Compaction Effort

## Slide 18
2. Effect of Compaction Effort
The standard Proctor mold and hammer were used to obtain these compaction curves.
For all cases the number of layers was equal to 3.
For the standard Proctor test
Note:
As the compaction effort increases, d(max) increases and OMC decreases.
Standard
It is equal to the energy transferred (or work done) to an object when a force of one newton acts on that object in the direction of its motion through a distance of one meter (1 newton meter or N·m).
Notes: CE 382 Geotechnical Engineering I

## Slide 19: Example 1
For the five compaction tests shown in the table below find: (a) the maximum dry unit weight of crushed limestone fill to be used as road base material, (b) its OMC, and (c) the moisture range for 95% of standard Proctor.
Recall
V = 1/30 ft3
1 ft =30.48 cm

## Slide 20: Example 2
Find (a) The dry unit weight and water content at 95% standard Proctor; (b) The degree of saturation at maximum dry unit weight, and (c) plot the zero air voids line.
Gs= 2.7
Moist unit weight is directly given

## Slide 21: Example 3

## Slide 22: Example 3 (Cont.)

## Slide 23
Modified Proctor Test (ASTM D-1557, AASHTO T-180)
With the development of heavy rollers (also requirements of heavy aircrafts and trucks) and their use in field compaction, the standard Proctor test was modified for better representation of the field conditions. This is sometimes referred to as modified Proctor test.
Mold 1/30 ft3 in volume (same as for standard test)
5 layers
25 blows (same as for standard test)
10 lb hammer
18 inch drop
Developed in WWII by U.S. Army Corps of Engineers to better represent the compaction required for airfield to support heavy aircraft.

## Slide 24: Modified Proctor Test
Layer 1
Layer 2
Layer 3
Layer 4
Layer 5
Drop = 457.2 mm
(18 in)
Drop = 304.8 mm
(12 in)
hammer
= 2.5 kg (5.5 lb)
hammer
= 4.9 kg (10 lb)

## Slide 26
Because it increases compactive effort, the modified Proctor test results in an increase of the maximum dry unit weight of the soil, and this is accompanied by decrease in the optimum moisture content.
Compaction Energy for Unit Volume of Soil
Standard Proctor Test
Modified Proctor Test
Note: In the field, compactive effort is the number of passes of the roller of a certain type and weight on a given volume of soil.
Notes: CE 382 Geotechnical Engineering I

## Slide 28
Field Compaction
Most of the compaction in the field is done by means of ROLLERS.
The most common types are:
1. Smooth-wheel rollers (smooth-drum roller)
Up to 380 kPa
100% coverage
Not good for thick layers

## Slide 29
2. Pneumatic rubber-tired rollers
Up to 700 kPa
70% - 80% coverage
Combination of pressure and kneading

## Slide 30
3. Sheepsfoot rollers
Most effective in compacting clayey soils
7000 kPa

## Slide 31
4. Vibratory rollers
Efficient in compacting granular soils
Vibrators can be attached to smooth-wheel, pneumatic rubber-tired, or sheepsfoot rollers to provide vibratory effects to the soil.

## Slide 32
Handheld vibratory plates can be used for effective compaction of granular soils over a limited area.
5. Handheld vibratory

## Slide 33
Factors to be considered
w%
Soil type
Thickness of lift
Intensity of the pressure applied by the compacting equipment
The area over which the pressure is applied
No. of roller passes
There are several factors that must be considered to achieve the desired unit weight of compaction in the field:

## Slide 34
Relationship between dry unit weight and number of passes
Relationship between dry unit weight, number of passes, depth.
Lack of confining pressure towards the surface
Important thickness of lifts

## Slide 35
Establishing Field Specification
Specifications for Field Compaction

## Slide 36
Compaction Control

## Slide 37
Usually it is required for the contractor to achieve a compacted field dry unit weight of say 90 to 95% of the maximum dry unit weight determined in the laboratory by either the standard or modified Proctor test (Recall previous examples).
Relative compaction, R
For granular soils, specifications can be expressed in terms of relative density.
where
Approximate formula for granular soils
Applicable if the soil contains less than 12% fines (passing No. 200 sieve)
(a)
(b)
From (a) and (b)

## Slide 38
Economy and compaction
The contractor is expected to reach the minimum dry unit weight regardless of the field procedure adopted
Specification

## Slide 39
Determination of Field Unit Weight of Compaction
Common Methods:
1. Sand cone method (ASTM Designation D-1556)
W1 = weight of the jar, the cone, and the sand filling the jar
Filling the jar with very uniform dry Ottawa sand
Excavating a small hole in the area where the soil has been compacted
W2 = weight of the moist soil excavated from the hole.
W3 = the dry weight of the soil =
 = moisture content
We know that both relative compaction or relative density are both need determination of dry density in the field.
Recall
 = Ww/Ws

## Slide 40
W4 = combined weight of the jar, the cone, and the remaining sand filling the jar.
W5 = weight of sand to fill the hole and cone
V = the volume of the excavated hole
The cone with the sand-filled jar attached to it is inverted and placed over the hole.
Wc= weight of sand to fill the cone only
The dry unit weight of compaction made in the field is determined as

## Slide 41
2. Rubber Balloon Method (ASTM Designation D-2167)
Similar to sand cone method except that the volume of the hole is determined by introducing into it a rubber balloon filled with water from a calibrated vessel.

## Slide 42
3. Nuclear Method
Nuclear density meter (Densometer)
Measures the weight of wet soil per unit volume and the weight of water present in a unit volume of soil.
The dry unit weight of compacted soil can be determined by subtracting the weight of water from the moist unit weight of soil.
Dense soil absorbs more radiation than loose soil.
ASTM D6938 - 15
Standard Test Methods for In-Place Density and Water Content of Soil and Soil-Aggregate by Nuclear Methods (Shallow Depth).