## Slide 1: By Dr. Saied Darwish (Prof. Industrial Engineering Department, KSU)
The Selection of
Manufacturing Engineering Processes

## Slide 2
CONTENTS
CHAPTER ONE: Fits and Tolerances
CHAPTER TWO: Fundamental of metal cutting
CHAPTER THREE: Mechanics of metal cutting
CHAPTER FOUR: Tool wear and tool life
CHAPTER FIVE: Drilling
CHAPTER SIX: Milling
CHAPTER SEVEN : Grinding
CHAPTER EIGHT: Broaching

## Slide 3
CHAPTER SEVEN
GRINDING OPERATION
7
CHAPTER SEVEN: Grinding Operation
CONTENTS

## Slide 4
7.1 Grinding operation
Grinding is a material removal process in which abrasive particles are bonded to form a grinding wheel that operates at very high surface speeds.
The grinding wheel is precisely balanced for high rotational speeds.
Grinding may be linked to the milling process: Cutting occurs on either the periphery or the face of the grinding wheel, similar to peripheral milling and face milling. Figure 7.1
CHAPTER SEVEN: Grinding Operation

## Slide 5
CHAPTER SEVEN: Grinding Operation
Figure 7.1: (a) The geometry of surface grinding, showing cutting conditions; (b) assumed longitudinal shape and (c) cross-section of a single chip.

## Slide 6
7.2 Significant differences between grinding and milling
The abrasive grains in the wheel are much smaller than the teeth on the milling cutter.
Cutting speeds in grinding are much higher than in milling.
A grinding wheel is self sharpening (as the wheel wears, the abrasive particles become dull and either fracture to create fresh cutting edges or are pulled out of the surface of the wheel to expose new grains).
CHAPTER SEVEN: Grinding Operation

## Slide 7
7.3 The grinding wheel
The grinding wheel consists of abrasive particles and bonding materials.
The bonding material holds particles in place and establishes the structure and shape of the wheel.
CHAPTER SEVEN: Grinding Operation

## Slide 8
7.4 Abrasive material
General properties of an abrasive material used in grinding wheels include high hardness, wear resistance, and toughness.
The abrasive materials of greatest commercial importance are:
Aluminum oxide (Al2O3)
Silicon carbide (SiCa)
Cubic boron nitride (CBN)
Diamond (natural and synthetic)
CHAPTER SEVEN: Grinding Operation

## Slide 9
7.5 Grain size
There are two main grain sizes available:
Small grain size: suitable for grinding hard materials, with better surface finish.
Large grain size is suitable for grinding soft materials with high material removal rate.
CHAPTER SEVEN: Grinding Operation

## Slide 10
7.6 Bonding materials
The bonding material must be able to withstand centrifugal forces and high temperatures.
Following are some common bonding materials:
Vitrified bond (clay and ceramic materials)
Silicate bond (sodium silicate)
Rubber bond
Metallic bond (usual bond)
CHAPTER SEVEN: Grinding Operation
Notes: Vitrified: مزجّج

## Slide 11
7.6 Cont. Bonding materials
CHAPTER SEVEN: Grinding Operation
Notes: Vitrified: مزجّج

## Slide 12
7.7 Standard grinding wheel shapes
Grinding wheels are available in different shapes,
in figure some standard grinding wheel shapes
are shown.
CHAPTER SEVEN: Grinding Operation
Figure 7.2: Some standard grinding wheel shapes: (a) straight, (b) recessed two sides, (c) metal wheel frame with abrasive bonded to outside circumference, (d) abrasive cutoff wheel, (e) cylinder wheel, (f) straight cup wheel, and (g) flaring cup wheel

## Slide 13
7.8 Dressing of grinding wheel
As the wheel is used, there is a tendency for the wheel to become loaded with metallic chips and the grains become dull or glaze. To improve the condition of the wheel a process termed “wheel dressing” is used as shown in figure 7.3.
CHAPTER SEVEN: Grinding Operation
Figure7.3: Schematic arrangement of stick dressing.

## Slide 14
7.9 Truing of grinding wheel
Grinding wheels lose their geometry during use. Truing operation restores the original shape. A single point diamond tool is used to true the wheel as shown in figure 7.4.
CHAPTER SEVEN: Grinding Operation
Figure 7.4: Diamond nibs may be used for truing wheels in batch operations

## Slide 15
7.10 Grinding operations and grinding machines
7.10.1 Cylindrical grinding:
Cylindrical grinding as its name suggests, is used for rotational parts. These grinding operations are divided into two basic types.
External cylindrical grinding which is similar to external turning. The grinding machine used for these operations closely resemble a lathe in which the tool post has been replaced by a high speed motor to rotate the grinding wheel.
Internal cylindrical grinding operates somewhat like a boring operation. The workpiece is usually held in a chuck and rotated to provide surface speed. The wheel is fed in either of two ways: (1) traverse feed or (2) plunge feed
CHAPTER SEVEN: Grinding Operation

## Slide 16
CHAPTER SEVEN: Grinding Operation
Figure 7.5: Two types of cylindrical grinding: (a) external and (b) internal

## Slide 17
7.10 Grinding operations and grinding machines
7.10.1 Cylindrical grinding:
traverse feed: grinding wheel is fed in a direction parallel to the axis of rotation of the workpiece
plunge feed: plunge cut, the grinding wheel is fed radially into the work
CHAPTER SEVEN: Grinding Operation

## Slide 18
CHAPTER SEVEN: Grinding Operation
Figure 7.6: Two types of feed motion in external cylindrical: (a) traverse feed and (b) plunge-cut.

## Slide 19
7.10.2 Surface grinding
Surface grinding is normally used to grind plain flat surfaces. It is performed using either the periphery of the grinding wheel or the flat face of the wheel.
Four types of surface grinding machines are used in surface grinding operation.
horizontal spindle with reciprocating worktable
horizontal spindle with rotating worktable
vertical spindle with reciprocating worktable
vertical spindle with rotating worktable.
CHAPTER SEVEN: Grinding Operation

## Slide 20
CHAPTER SEVEN: Grinding Operation
Figure 7.7: Four types of surface grinding: (a) horizontal spindle with reciprocating worktable, (b) horizontal spindle with rotating worktable, (c) vertical spindle with reciprocating worktable, and (d) vertical spindle with rotating worktable.

## Slide 21
7.10.3 Centerless grinding
Centerless grinding has a number of advantages over cylindrical grinding.
It is self-centering, the stock removal rate is higher, and the work is firmly held by the support plate and control or regulating wheel, which results in better dimensional accuracy
CHAPTER SEVEN: Grinding Operation
Figure 7.8: External centerless grinding

## Slide 22
CHAPTER SEVEN: Grinding Operation
Figure 7.9: Internal centerless grinding.

## Slide 23
7.11 Forces and power in grinding
There are three force components involved in the grinding operation
Pr = Radial force, Pa = Axial force, Ps = Main cutting force (Tangential force).
CHAPTER SEVEN: Grinding Operation
Figure 7.10: Force components in grinding.
The power can be calculated from the following formula.
(kW)

## Slide 24
7.12 Related abrasive processes
7.12.1 Honing
Honing is an abrasive process performed by a set of bonded abrasive sticks.
A common application is to finish the bores of internal combustion engines, other applications
CHAPTER SEVEN: Grinding Operation
Figure 7.11: The honing process: (a) the honing tool used for internal bore surfaces
(b) cross hatched surface pattern created by the action of the honing tool.

## Slide 25
7.12.2 Lapping
Lapping is an abrasive process used to produce surface finish of extreme accuracy and smoothness. It is used in the production of optical lenses, metallic bearing surfaces and gauges
CHAPTER SEVEN: Grinding Operation
Figure 7.12: The lapping process in lens making.

## Slide 26
7.12.3 Super finishing
Super finishing is an abrasive process similar to honing. Super finishing differ from honing in the following aspects:
The strokes are shorter.
High frequencies are used.
Lower pressure is applied between the tool and surface.
The grit size are smaller.
Workpiece speed is slower.
CHAPTER SEVEN: Grinding Operation

## Slide 27
The result of these conditions is mirror like finishes. This process can be used to finish flat and external cylindrical surfaces, as shown in figure 7.13.
CHAPTER SEVEN: Grinding Operation
Figure 7.13: Super finishing on an external cylindrical surface.