## Slide 1: Adventures in Crystal Growth
1/20/2011 NRC Canadian Neutron Beam Centre Seminar

## Slide 2: Overview
Why grow crystals?
Crystal Growth Techniques

## Slide 3: Single Crystals
Macroscopic samples with long-range
alignment of periodic atomic structure
cf.
“powder” samples – many randomly oriented microscopic “crystallites”
“liquid” / amorphous - no long-range order

## Slide 4: Why grow crystals?
Anisotropic properties / direction dependence
  Easy/hard magnetization axes
  Anisotropic transport properties
  Determine crystal, magnetic structure, Fermi surface
  ab plane vs. c-axis properties in layered materials
Minimize effects of grain boundaries
Minimize effects of long-range disorder
Rejection of impurity phases / off-stoichiometry
They’re pretty to look at!

## Slide 5: Why grow crystals?
Specific to neutron / x-ray scattering
  In powders/liquids, signals are spread into cones.
  Only direction-averaged |Q| available
    Loss of information!
    Direction-dependent signal of interest spread out & convolved with uninteresting signals from other directions!

## Slide 6: Why wouldn’t you grow crystals?
Very time consuming, labor intensive
  Powders are much easier to make!
Lots of variables in “recipe” to be determined
  Method to use, temperature, pressure, atmosphere, cooling rate, crucible material, choice of flux / solvent, choice of starting compounds, control oxygen content, doping levels, size/shape of starting materials, optimize for desired crystal size / orientation.
Can it even be grown?
Requires specialized equipment
  Special furnaces, characterization lab
May not be able to reach necessary temperature
May not be able to reach necessary pressure
May crack / evaporate / decompose / incorporate H2O
Special atmospheres may be needed
May form other phases instead
May have large stress/strain, defects

## Slide 7: Basic plan
  0. Decide what to make
  Educated guess: Can it be grown? Is it worth the effort?
  Make powder sample of desired material
    Solid state reaction in furnace?
    Wet chemistry methods?
  Characterize powder
    XRD, resistivity, susceptibility, TGA, etc.
  If powder’s good, make crystal from it
    What method?
    Start with small “pilot” sample?
    Optimize recipe
  Characterize crystal
    Optical, XRD, resistivity, susceptibility, TGA, etc.
    Make bigger sample?
  Definitive measurements
    Synchrotron, neutrons, muons, NMR, ARPES…
  Publish!

## Slide 8: Crystal Growth Techniques
1. Growth from solution
  Idea: homogeneous soln -> solid xtals + solvent
2. Growth from gas (vapor) phase
  Idea: Evaporate powder, deposit vapor onto seeds
3. Growth from liquid (melt) phase
  Idea: Melt polyxtals of desired materials, slowly cool

## Slide 9: Crystal Growth Techniques
1. Growth from solution
  Idea: homogeneous soln -> solid xtals + solvent
2. Growth from gas (vapor) phase
  Idea: Evaporate powder, deposit vapor onto seeds
3. Growth from liquid (melt) phase
  Idea: Melt polyxtals of desired materials, slowly cool

## Slide 10: Crystal Growth from Solution
Simplest case: aqueous solution
  Needs: water-soluble, low temperature reaction
  Increased temps by applying pressure: “hydrothermal”
Organic solvents?
More general: flux growth
  Effect: by adding flux to material of interest, melting point is lowered.
  e.g. “eutectic,” “peritectic” points
  Heat until liquid state achieved, then cool very slowly
  Goal: desired material precipitates out (better if homogeneous!), excess flux separated out

## Slide 11: Flux method
Assemble stoichiometric quantities of desired materials, mix thoroughly
Choose an appropriate flux
  How much? (refer to phase diagrams, if available!)
Put sample materials + flux in crucible
Special choice of atmosphere?
Heat to liquid state
Cool very slowly
Separate precipitated sample from flux

## Slide 12: Flux Method
Choice of flux:
  Readily dissolves sample material
  Lowers melting point into achievable range
  High boiling point, “low” vapor pressure
  Dissolves sample homogeneously?
  Commercially available, minimal hazards
  Separates from sample material on cooling
  Typical choices: Ga, In, Sn, Pb, Sb, Bi, low melting halides or oxides
    “Self flux” also commonly used!
Choice of crucible:
  Very high melting point
  Does not react with sample
  Does not react with flux
  Typical choices: Al2O3, ZrO2, ThO2, Pt, Ta, Nb
Choice of environment / atmosphere
  What temperature?
  What cooling rate?
  Can it be done in air?
  If not, seal sample/flux/crucible in quartz tube with desired atmosphere
    Inert? Reducing? Oxidizing? Vacuum? What pressure?

## Slide 13: Flux Method
Advantages:
  Very good for alloys / intermetallics
    Including FeAs-based superconductors!
  Low stress/strain
  Good choice of flux lowers required temperatures
  Reduced need for specialized equipment
Disadvantages:
  Need for extended temperature control
  Usually get many small crystals – poor nucleation control
  Must be able to find suitable flux
  Must be able to find suitable crucible
  Must remove excess flux

## Slide 14
Sealed quartz container
Crucibles
Quartz wool
Sample + Flux

## Slide 15: Crystal Growth Techniques
1. Growth from solution
  Idea: homogeneous soln -> solid xtals + solvent
2. Growth from gas (vapor) phase
  Idea: Evaporate powder, deposit vapor onto seeds
3. Growth from liquid (melt) phase
  Idea: Melt polyxtals of desired materials, slowly cool

## Slide 16: Crystal Growth from Vapor Phase
Sublimation
Chemical Vapor Transport
Pulsed Laser Deposition
Metal-Organic Chemical Vapor Deposition
Container
Starting
Material
Vapor
Substrate or
Seed Crystal

## Slide 17: Crystal Growth from Vapor Phase
Useful for growing epitaxial thin films!
Issues:
  Need high vapor pressure / ability to evaporate
  Need substrate/seed onto which to grow crystal?
  Often quite slow
  Will vapor react with container?
  Need for specialized equipment

## Slide 18: Crystal Growth Techniques
1. Growth from solution
  Idea: homogeneous soln -> solid xtals + solvent
2. Growth from gas (vapor) phase
  Idea: Evaporate powder, deposit vapor onto seeds
3. Growth from liquid (melt) phase
  Idea: Melt polyxtals of desired materials, slowly cool

## Slide 19: Crystal Growth from Liquid (Melt)
Idea:
  Prepare polycrystalline sample
  Heat to above melting point
  Cool very slowly
  ***Lots of “tricks” to do this!***
Advantages:
  Can grow large crystals!
  Usually better control over nucleation
  Usually better control over shape of final product
  Good control over growth rates
Issues:
  Melting pt can be very high!
  Special atmosphere or vacuum needed?
  Xtals may grow with significant stress/strain
  Does it evaporate too quickly?
  Will it react with crucible / container?
  May not grow at all!
  May grow different phase from expected!

## Slide 20: Crystal Growth from Liquid (Melt)
Variety of techniques (“tricks”):
  Verneuil (“flame fusion”) ~early 1900’s
  Czochralski (“pulling”) ~1910’s
  Kyropoulos (“top seeding”) ~1920’s
  Bridgman (“directional solidification”) ~1940’s
  Skull Melting ~1970’s
  Laser-heated pedestal growth ~1990’s
  Micropulling ~1990’s
  Floating Zone (incl. image furnace) ~1990’s

## Slide 21: Verneuil Process
First used ~1902-1910 for large-scale sapphire / ruby growth (Al2O3)
O2 + Al2O3 inlet
O2 + H2 mix and ignite, T > 2000K
Molten drops fall onto “pedestal”
xtal forms & grows
Example of Al2O3 xtal (right end)

## Slide 22: Czochralski method
Developed 1917, Jan Czochralski
Start w/ seed xtal
Dip seed into melt
Slowly raise seed as it rotates
Used for industrial SC’s: Si, Ge
metals: Pd, Pt, Ag, Au
Some salts

## Slide 23: Bridgman-Stockbarger method
Bridgman, 1940’s
Idea: use temperature gradient to influence direction of xtal growth
Requires 2-zone furnace, accurate position / temperature control
Can grow some xtals with fewer impurities than Czochralski
e.g. GaAs
Bridgman
Stockbarger

## Slide 24: Skull Melting
Idea: MP too high for any crucible
Make sample act as own crucible!
Make large cylinder of desired material
Interior heated by RF induction
Cool exterior with flowing H2O in “fingers”
Remove xtals from inside “skull”
Very large samples! ~kgs
Typical use: ZrO2

## Slide 25: Optical Floating Zone (Image) method
Idea: use optical focusing to create floating “hot zone”
By slowly advancing feed rod through zone, crystal grows on seed rod
Can achieve very high temperatures up to ~2800K

## Slide 26: Optical Floating Zone (Image) method
Photo credit: G. Balakrishnan, U. Warwick

## Slide 27: Examples of Float-Zone crystals
courtesy K. Conder, PSI / ETH-Zurich

## Slide 28: Growth example: YBa2Cu3O7-
R. Liang, UBC
Crucible material:
BaZrO3
Starting materials: Y2O3 + BaCO3 + CuO →

## Slide 29: Summary
“There are many ways to skin a cat…”
… this is both a blessing and a curse!
Substantial progress in recent years
Availability of high-quality crystals = Ability to extract high-quality scientific results!