Reline Procedures for Complete Dentures

Before impressioning remove all acrylic undercuts inside of denture with a Brasseler bur.

Impression per your instructors instructions (border moulding, polysulfide wash,  etc.). Take opposing alginate and bite registration.

Box impression taking care to bead with rope wax no further than 3 mm from peripheries, and pour with labstone. DO NOT SEPARATE YET!

Mount casts on articlator using bite registration.Be sure incisal pin is flush with top of articulator.

Optional: Mount denture in reline jig  instead of articulator.

Carefully remove denture from cast. Do not break the ridge off the cast (This is why you relieved the undercuts from the inside of the denture prior to impressioning).

Remove all impression material and adhesive. Reduce peripheries of denture by 3-4 mm and reduce tissue side of denture acrylic at least a couple millimeters (unless  you did this  prior to impressioning). Optional- remove palate of maxillary denture with bur. Place posterior palatal seal on maxillary denture cast!

Place denture back onto cast on articulator and sticky wax  denture teeth to occlude with opposing. There should be a gap between denture and edentulous cast/

Wax denture to cast filling buccal and facial  peripheries with baseplate wax, wax and seal lingual peripheries and any other unwaxed areas, sealing denture to cast completely (including replacing palate of maxillary denture if you removed it).

Remove cast from  articulator, flask, and boilout. DO not paint separator on denture.

Turn in to lab with work authorization for packing of acrylic and curing.

Receive in 2 days, on cast, for finishing and polishing.