## Slide 1: Chapter 15: Characteristics & Applications of Polymers
<number>
ISSUES TO ADDRESS...
• What are the tensile properties of polymers and how are they affected by basic microstructural features?
• Hardening, anisotropy, and annealing in polymers.
• How does the elevated temperature mechanical
response of polymers compare to ceramics and metals?
Notes: <number>

## Slide 2: Mechanical Properties of Polymers – Stress-Strain Behavior
<number>
• Fracture strengths of polymers ~ 10% of those for metals
• Deformation strains for polymers > 1000% – for most metals, deformation strains < 10%
brittle polymer
plastic
elastomer
elastic moduli – less than for metals
Adapted from Fig. 15.1, Callister & Rethwisch 9e.
Notes: <number>
<number>

## Slide 3: Mechanisms of Deformation—Brittle Crosslinked and Network Polymers
<number>
brittle failure
plastic failure
e
x
x
aligned, crosslinked
polymer
Stress-strain curves adapted from Fig. 15.1, Callister & Rethwisch 9e.
Initial
Near Failure
Initial
network polymer
Near Failure
σ(MPa)
Notes: <number>
<number>

## Slide 4: Mechanisms of Deformation — Semicrystalline (Plastic) Polymers
<number>
brittle failure
plastic failure
σ(MPa)
x
x
crystalline
block segments
separate
fibrillar structure
near
failure
crystalline
regions align
onset of
necking
undeformed
structure
amorphous
regions
elongate
unload/reload
Stress-strain curves adapted from Fig. 15.1, Callister & Rethwisch 9e. Inset figures along plastic response curve adapted from Figs. 15.12 & 15.13, Callister & Rethwisch 9e. (From SCHULTZ, POLYMER MATERIALS SCIENCE, 1st Edition, © 1974. Reprinted by permission of Pearson Education, Inc., Upper Saddle River, NJ.)1974, pp 500-501.)
e
Notes: <number>
<number>

## Slide 5: Predeformation by Drawing
<number>
• Drawing…(ex: monofilament fishline)
-- stretches the polymer prior to use
-- aligns chains in the stretching direction
• Results of drawing:
-- increases the elastic modulus (E) in the
stretching direction
-- increases the tensile strength (TS) in the
stretching direction
-- decreases ductility (%EL)
• Annealing after drawing...
-- decreases chain alignment
-- reverses effects of drawing (reduces E and TS, enhances %EL)
• Contrast to effects of cold working in metals!
Adapted from Fig. 15.13, Callister & Rethwisch 9e. (From Schultz, Polymer Materials Science, 1st Edition, © 1974. Reprinted by permission of Pearson Education, Inc., Upper Saddle River, NJ.)1974, pp 500-501.)
Notes: <number>
<number>

## Slide 6: Mechanisms of Deformation—Elastomers
<number>
• Compare elastic behavior of elastomers with the:
-- brittle behavior (of aligned, crosslinked & network polymers), and
-- plastic behavior (of semicrystalline polymers)
(as shown on previous slides)
Stress-strain curves adapted from Fig. 15.1, Callister & Rethwisch 9e. Inset figures along elastomer curve (green) adapted from Fig. 15.15, Callister & Rethwisch 9e. (Fig. 15.15 adapted from Z. D. Jastrzebski, The Nature and Properties of Engineering Materials, 3rd edition. Copyright © 1987 by John Wiley & Sons, New York. Reprinted by permission of John Wiley & Sons, Inc.)
initial: amorphous chains are
kinked, cross-linked.
x
final: chains
are straighter,
still
cross-linked
elastomer
deformation
is reversible (elastic)!
brittle failure
plastic failure
x
x
σ(MPa)
e
Notes: <number>
<number>

## Slide 7: Thermoplastics vs. Thermosets
<number>
<number>
• Thermoplastics:
-- little crosslinking
-- ductile
-- soften w/heating
-- polyethylene
polypropylene
polycarbonate
polystyrene
• Thermosets:
-- significant crosslinking
(10 to 50% of repeat units)
-- hard and brittle
-- do NOT soften w/heating
-- vulcanized rubber, epoxies,
polyester resin, phenolic resin
Adapted from Fig. 15.19, Callister & Rethwisch 9e. (From F. W. Billmeyer, Jr., Textbook of Polymer Science, 3rd edition. Copyright © 1984 by John Wiley & Sons, New York. Reprinted by permission of John Wiley & Sons, Inc.)
Callister,
Fig. 16.9
T
Molecular weight
Tg
Tm
mobile
liquid
viscous
liquid
rubber
tough
plastic
partially
crystalline
solid
crystalline
solid
Notes: <number>
<number>

## Slide 8: Influence of T and Strain Rate on Thermoplastics
<number>
<number>
• Decreasing T...
-- increases E
-- increases TS
-- decreases %EL
• Increasing
strain rate...
-- same effects
as decreasing T.
Adapted from Fig. 15.3, Callister & Rethwisch 9e. (Reprinted with permission from T. S. Carswell and H. K. Nason, “Effect of Environmental Conditions on the Mechanical Properties of Organic Plastics,” in Symposium on Plastics. Copyright ASTM International, 100 Barr Harbor Drive, West Conshohocken, PA 19428.)
20
4
0
6
0
8
0
0
0
0.1
0.2
0.3
4ºC
20ºC
40ºC
60ºC
to 1.3
Plots for
semicrystalline
PMMA (Plexiglas)
σ(MPa)
e
Notes: <number>
<number>

## Slide 9: Melting & Glass Transition Temps.
<number>
What factors affect Tm and Tg?
Both Tm and Tg increase with increasing chain stiffness
Chain stiffness increased by presence of
  Bulky sidegroups
  Polar groups or sidegroups
  Chain double bonds and aromatic chain groups
Regularity of repeat unit arrangements – affects Tm only
Adapted from Fig. 15.18, Callister & Rethwisch 9e.
Notes: <number>
<number>

## Slide 10: Time-Dependent Deformation
• Representative Tg values (C):
PE (low density)
PE (high density)
PVC
PS
PC
- 110
- 90
+ 87
+100
+150
Selected values from Table 15.2, Callister & Rethwisch 9e.
<number>
• Stress relaxation test:
-- strain in tension to e and hold.
-- observe decrease in
stress with time.
• Relaxation modulus:
time
strain
tensile test
eo
σ(t)
• There is a large decrease in Er
for T > Tg.
(amorphous
polystyrene)
Fig. 15.7, Callister & Rethwisch 9e. (From A. V. Tobolsky, Properties and Structures of Polymers. Copyright © 1960 by John Wiley & Sons, New York. Reprinted by permission of John Wiley & Sons, Inc.)
10
3
10
1
10
-1
10
-3
10
5
60
100
140
180
rigid solid
(small relax)
transition
region
T(ºC)
Tg
Er (10 s)
in MPa
viscous liquid
(large relax)
Notes: <number>
<number>

## Slide 11: Crazing During Fracture of Thermoplastic Polymers
<number>
fibrillar bridges
microvoids
crack
aligned chains
Craze formation prior to cracking
– during crazing, plastic deformation of spherulites – and formation of microvoids and fibrillar bridges
Fig. 15.9, Callister & Rethwisch 9e. (From J. W. S. Hearle, Polymers and Their Properties, Vol. 1, Fundamentals of Structure and Mechanics, Ellis Horwood, Ltd., Chichester, West Sussex, England, 1982.)
Notes: <number>
<number>
  Note: crack spreads by breaking C-C bonds
Ductile plastics have large craze zones that absorb large amounts of energy as it spreads

## Slide 12: Polymer Types – Fibers
<number>
Fibers - length/diameter >100
Primary use is in textiles.
Fiber characteristics:
  high tensile strengths
  high degrees of crystallinity
  structures containing polar groups
Formed by spinning
  extrude polymer through a spinneret (a die containing many small orifices)
  the spun fibers are drawn under tension
  leads to highly aligned chains - fibrillar structure
Notes: <number>
<number>

## Slide 13: Polymer Types – Miscellaneous
<number>
Coatings – thin polymer films applied to surfaces – i.e., paints, varnishes
  protects from corrosion/degradation
  decorative – improves appearance
  can provide electrical insulation
Adhesives – bonds two solid materials (adherands)
  bonding types:
    Secondary – van der Waals forces
    Mechanical – penetration into pores/crevices
Films – produced by blown film extrusion
Foams – gas bubbles incorporated into plastic
Notes: <number>
<number>

## Slide 14: Advanced Polymers
<number>
Molecular weight ca. 4 x 106 g/mol
Outstanding properties
  high impact strength
  resistance to wear/abrasion
  low coefficient of friction
  self-lubricating surface
Important applications
  bullet-proof vests
  golf ball covers
  hip implants (acetabular cup)
UHMWPE
Adapted from chapter-opening photograph, Chapter 22, Callister 7e.
Ultrahigh Molecular Weight Polyethylene (UHMWPE)
Notes: <number>
<number>

## Slide 15: Advanced Polymers
<number>
styrene
butadiene
Thermoplastic Elastomers
Styrene-butadiene block copolymer
hard component domain
soft component domain
Fig. 15.22, Callister & Rethwisch 9e.
Fig. 15.21(a), Callister & Rethwisch 9e.
Notes: <number>

## Slide 16: Summary
<number>
• Limitations of polymers:
-- E, σy, Kc, Tapplication are generally small.
-- Deformation is often time and temperature dependent.
• Thermoplastics (PE, PS, PP, PC):
-- Smaller E, σy, Tapplication
-- Larger Kc
-- Easier to form and recycle
• Elastomers (rubber):
-- Large reversible strains!
• Thermosets (epoxies, polyesters):
-- Larger E, σy, Tapplication
-- Smaller Kc
Table 15.3 Callister & Rethwisch 9e:
Good overview
of applications
and trade names
of polymers.
Notes: <number>

## Slide 17: Summary
<number>
• Polymer applications
-- elastomers -- fibers
-- coatings -- adhesives
-- films -- foams
-- advanced polymeric materials
Notes: <number>

## Slide 18: ANNOUNCEMENTS
<number>
Core Problems:
Self-help Problems:
Reading:
Notes: <number>