## Slide 1: Crystallization
Crystallization is the (natural or artificial) process of formation of solid crystals precipitating from a solution, melt or more rarely deposited directly from a gas .
Crystallization is also a chemical solid–liquid separation technique, in which mass transfer of a solute from the liquid solution to a pure solid crystalline phase occurs.

## Slide 2
Crystallization is therefore an aspect of precipitation, obtained through a variation of the solubility conditions of the solute in the solvent , as compared to precipitation due to chemical reaction.

## Slide 3: Precipitation
is the formation of a solid in a solution or inside another solid during a chemical reaction or by diffusion in a solid. When the reaction occurs in a liquid, the solid formed is called the precipitate, or when compacted by a centrifuge, a pellet. The liquid remaining above the solid is in either case called the supernate or supernatant.

## Slide 4
An important stage of the precipitation process is the onset of nucleation. The creation of a hypothetical solid particle includes the formation of an interface, which requires some energy based on the relative surface energy of the solid and the solution. If this energy is not available, and no suitable nucleation surface is available, supersaturation occurs.

## Slide 5
The crystallization process consists of two major events, nucleation and crystal growth.
Nucleation is the step where the solute molecules dispersed in the solvent start to gather into clusters, on the nanometer scale (elevating solute concentration in a small region), that become stable under the current operating conditions.

## Slide 6
However, when the clusters are not stable, they redissolve. Therefore, the clusters need to reach a critical size in order to become stable nuclei. Such critical size is dictated by the operating conditions (temperature, supersaturation, etc.).

## Slide 7
It is at the stage of nucleation that the atoms arrange in a defined and periodic manner that defines the crystal structure — note that "crystal structure" is a special term that refers to the relative arrangement of the atoms, although those are a result of the internal crystal structure.

## Slide 8: The crystal Growth
The crystal growth is the subsequent growth of the nuclei that succeed in achieving the critical cluster size. Nucleation and growth continue to occur simultaneously while the supersaturation exists. Supersaturation is the driving force of the crystallization, hence the rate of nucleation and growth is driven by the existing supersaturation in the solution.

## Slide 9
Once the supersaturation is exhausted, the solid–liquid system reaches equilibrium and the crystallization is complete.

## Slide 10
Artificial methods
For crystallization (recrystallization) to occur from a solution it must be supersaturated. This means that the solution has to contain more solute entities (molecules or ions) dissolved than it would contain under the equilibrium (saturated solution).
This can be achieved by various methods, with (1) solution cooling, (2) addition of a second solvent to reduce the solubility of the solute (technique known as antisolvent or drown-out), (3) chemical reaction and (4) change in pH being the most common methods used in industrial practice. Other methods, such as solvent evaporation, can also be used.

## Slide 11: Recrystallization
Single-solvent recrystallization
Typically, the mixture of "compound A" and "impurity B" are dissolved in the smallest amount of hot solvent to fully dissolve the mixture, thus making a saturated solution. The solution is then allowed to cool. As the solution cools the solubility of compounds in solution drops. This results in the desired compound dropping (recrystallizing) from solution. The slower the rate of cooling, the bigger the crystals formed.

## Slide 12
Multi-solvent recrystallization
This method is the same as the above but where two (or more) solvents are used. This relies on both "compound A" and "impurity B" being soluble in a first solvent.
A second solvent is slowly added. Either "compound A" or "impurity B" will be insoluble in this solvent and precipitate, whilst the other of "compound A"/"impurity B" will remain in solution. Thus the proportion of first and second solvents is critical.
Typically the second solvent is added slowly until one of the compounds begins to crystallize from solution and then the solution is cooled. Heating is not required for this technique but can be used

## Slide 15
Patterns are located upon the points of a Lattice, which is an array of points repeating periodically in three dimensions. The points can be thought of as forming identical tiny boxes, called unit cells, that fill the space of the lattice

## Slide 16: Unit cell
The crystal structure of a material or the arrangement of atoms within a given type of crystal structure can be described in terms of its unit cell. The unit cell is a small box containing one or more atoms, a spatial arrangement of atoms.

## Slide 17
.
.
Simple cubic (P)
Face-centered cubic (F)
Face-centered cubic (F)

## Slide 18
The unit cells stacked in three-dimensional space describe the bulk arrangement of atoms of the crystal. The crystal structure has a three dimensional shape.
The unit cell is given by its lattice parameters which are the length of the cell edges and the angles between them, while the positions of the atoms inside the unit cell are described by the set of atomic positions (xi , yi , zi) measured from a lattice point.

## Slide 19
A crystal's structure and symmetry play a role in determining many of its physical properties, such as cleavage, electronic band structure, and optical transparency.

## Slide 20
Mineralogy is the study of chemistry, crystal structure, and physical (including optical) properties of minerals. Specific studies within mineralogy include the processes of mineral origin and formation, classification of minerals, their geographical distribution, as well as their utilization.

## Slide 21
Crystallography is the experimental science of the arrangement of atoms in solids.
The word "crystallography" derives from the Greek words crystallon = cold drop / frozen drop, with its meaning extending to all solids with some degree of transparency, and grapho = write.
Before the development of X-ray diffraction crystallography (see below), the study of crystals was based on their geometry. This involves measuring the angles of crystal faces relative to theoretical reference axes
The atom is a basic unit of matter that consists of a dense, central nucleus surrounded by a cloud of negatively charged electrons.
The atomic nucleus contains a mix of positively charged protons and electrically neutral neutrons (except in the case of hydrogen-1, which is the only stable nuclide with no neutrons). The electrons of an atom are bound to the nucleus by the electromagnetic force. Likewise, a group of atoms can remain bound to each other, forming a molecule.

## Slide 22
An atom containing an equal number of protons and electrons is electrically neutral, otherwise it has a positive charge if there are less electrons (electron deficiency) or negative charge if there are more electrons (electron excess). A positively or negatively charged atom is known as an ion.
An atom is classified according to the number of protons and neutrons in its nucleus:
the number of protons determines the chemical element, and the number of neutrons determines the isotope of the element.[1]
The name atom comes from the Greek "ἄτομος"—átomos (from α-, "un-" + τέμνω – temno, "to cut"[2]), which means uncuttable, or indivisible, something that cannot be divided further.[3] The concept of an atom as an indivisible component of matter was first proposed by early Indian and Greek philosophers. In the 17th and 18th centuries, chemists provided a physical basis for this idea by showing that certain substances could not be further broken down by chemical methods. During the late 19th and early 20th centuries, physicists discovered subatomic components and structure inside the atom, thereby demonstrating that the 'atom' was divisible. The principles of quantum mechanics were used to successfully model the atom.[4][5]

## Slide 23
(crystallographic axes), and establishing the symmetry of the crystal in question. The former is carried out using a goniometer. The position in 3D space of each crystal face is plotted on a stereographic net, e.g. Wulff net or Lambert net. In fact, the pole to each face is plotted on the net. Each point is labelled with its Miller index. The final plot allows the symmetry of the crystal to be established.
Crystallographic methods now depend on the analysis of the diffraction

## Slide 24
patterns of a sample targeted by a beam of some type. Although X-rays are most commonly used, the beam is not always electromagnetic radiation. For some purposes electrons or neutrons are used. This is facilitated by the wave properties of the particles. Crystallographers often explicitly state the type of illumination used when referring to a method, as with the terms X-ray diffraction, neutron diffraction and electron diffraction.
These three types of radiation interact with the specimen in different ways. X-rays interact with the spatial distribution of the valence electrons, while electrons are charged particles and therefore feel the total charge distribution of both the atomic nuclei and the surrounding electrons. Neutrons are scattered by the atomic nuclei through the strong nuclear forces, but in addition, the magnetic moment of neutrons is non-zero. They are therefore also scattered by magnetic fields. When neutrons are scattered from hydrogen-containing materials, they produce diffraction patterns with high noise levels. However, the material can sometimes be treated to substitute hydrogen for deuterium. Because of these different forms of interaction, the three types of radiation are suitable for different crystallographic

## Slide 25
Miller indices
Main article: Miller index
Planes with different Miller indices in cubic crystals
Vectors and atomic planes in a crystal lattice can be described by a three-value Miller index notation (ℓmn). The ℓ, m and n directional indices are separated by 90°, and are thus orthogonal. In fact, the ℓ component is mutually perpendicular to the m and n indices.

## Slide 26
Considering only (ℓmn) planes intersecting one or more lattice points (the lattice planes), the perpendicular distance d between adjacent lattice planes is related to the (shortest) reciprocal lattice vector orthogonal to the planes by the formula:
By definition, (ℓmn) denotes a plane that intercepts the three points a1/ℓ, a2/m, and a3/n, or some multiple thereof. That is, the Miller indices are proportional to the inverses of the intercepts of the plane with the unit cell (in the basis of the lattice vectors). If one or more of the indices is zero, it simply means that the planes do not intersect that axis (i.e. the intercept is "at infinity").

## Slide 27
Miller indices are a notation system in crystallography for planes and directions in crystal (Bravais) lattices.
In particular, a family of lattice planes is determined by three integers ℓ, m, and n, the Miller indices. They are written (hkl), and each index denotes a plane orthogonal to a direction (h, k, l) in the basis of the reciprocal lattice vectors. By convention, negative integers are written with a bar, as in 3 for −3. The integers are usually written in lowest terms, i.e. their greatest common divisor should be 1. Miller index 100 represents a plane orthogonal to direction ℓ; index 010 represents a plane orthogonal to direction m, and index 001 represents a plane orthogonal to n.

## Slide 29
There are also several related notations[1]:
the notation {ℓmn} denotes the set of all planes that are equivalent to (ℓmn) by the symmetry of the lattice.
In the context of crystal directions (not planes), the corresponding notations are:
[ℓmn], with square instead of round brackets, denotes a direction in the basis of the direct lattice vectors instead of the reciprocal lattice; and

## Slide 30
similarly, the notation 〈hkl〉 denotes the set of all directions that are equivalent to [ℓmn] by symmetry.
Miller indices were introduced in 1839 by the British mineralogist William Hallowes Miller. The method was also historically known as the Millerian system, and the indices as Millerian,[2] although this is now rare.
The precise meaning of this notation depends upon a choice of lattice vectors for the crystal, as described below. Usually, three primitive lattice vectors are used. However, for cubic crystal systems, the cubic lattice vectors are used even when they are not primitive (e.g., as in body-centered and face-centered crystals).

## Slide 31: Bravais lattice
In geometry and crystallography, a Bravais lattice, studied by Auguste Bravais (1850),[1] is an infinite array of discrete points generated by a set of discrete translation operations described by:
R=n1a1+n2a2+n3a3
where ni are any integers and ai are known as the primitive vectors which lie in different planes and span the lattice. This discrete set of vectors must be closed under vector addition and subtraction. For any choice of position vector R, the lattice looks exactly the same.

## Slide 32
Bravais lattices in at most 2 dimensions
In each of 0-dimensional and 1-dimensional space there is just one type of Bravais lattice.
In two dimensions, there are five Bravais lattices. They are oblique, rectangular, centered rectangular (rhombic), hexagonal, and square.[2]

## Slide 34: Bravais lattices in 3 dimensions
The 14 Bravais lattices in 3 dimensions are arrived at by combining one of the seven lattice systems (or axial systems) with one of the lattice centerings. Each Bravais lattice refers to a distinct lattice type.
The lattice centerings are:
Primitive centering (P): lattice points on the cell corners only.
Body centered (I): one additional lattice point at the center of the cell.
Face centered (F): one additional lattice point at center of each of the faces of the cell.

## Slide 35
Base centered (A, B or C): one additional lattice point at the center of each of one pair of the cell faces.
Not all combinations of the crystal systems and lattice centerings are needed to describe the possible lattices. There are in total 7 × 6 = 42 combinations, but it can be shown that several of these are in fact equivalent to each other. For example, the monoclinic I lattice can be described by a monoclinic C lattice by different choice of crystal axes. Similarly, all A- or B-centered lattices can be described either by a C- or P-centering. This reduces the number of combinations to 14 conventional Bravais lattices, shown in the table below.

## Slide 36
triclinic | P |  |  | 
monoclinic | P | C |  | 
orthorhombic | P | C | I | F
tetragonal | P | I |  | 
rhombohedral | P |  |  | 
hexagonal | P |  |  | 
cubic | P (pcc) | I (bcc) | F (fcc) | 

## Slide 37
The volume of the unit cell can be calculated by evaluating a · b × c where a, b, and c are the lattice vectors. The volumes of the Bravais lattices are given below:

## Slide 38
Volume |  |  | 
Triclinic |  |  | 
Monoclinic |  |  | 
Orthorhombic | abc |  | 
Tetragonal | a2c |  | 
rhombohedral |  |  | 
Hexagonal |  |  | 
Cubic | a3 |  |