## Slide 1: Deflasking , Remounting and Occlusal Adjustment
Dr.Mohammad Al Sayed
16/3/2008

## Slide 2: Deflasking of the dentures
A-Removing the mold:
- after processing the acrylic resin denture the flask is cooled slowly to room temperature.
- remove the lid of the flask by prying with a knife .
- place the flask in an ejector press.
- using minimum pressure eject the mold from the flask.

## Slide 3
B-Removing the denture and cast :
- remove the stone cap ( the third layer ) by gently prying it off to expose the occlusal surfaces and incisal edges of the teeth.
- with a plaster saw make 4 cuts, 2 in canine region and 2 in the posterior region.
- with the plaster knife gently pry the sectioned plaster away from the facial surface of the teeth.
- after removing the outer sections of stone from the denture , trim the stone away from the lingual surfaces of the teeth before attempting to remove the inner section of plaster and stone.
this procedure will
a-prevent breaking the teeth
b-prevent lifting the denture from the cast

## Slide 4: - During deflasking: be careful to preserve the cast, also do not left or remove the denture from the casts
- Clean the denture and cast from plaster.
Remove any stone or bubbles from the exposed acrylic resin and from the occlusal surfaces of the teeth.
- Remove any particles of stone from the base of the cast and index grooves.
- Using a stiff brush , soap and water clean the denture and cast before starting the laboratory remount

## Slide 5: Laboratory remount procedure and selective grinding:
Objective: to correct errors in the occlusion due to slight changes in the position of the teeth that may have occurred during waxing, packing and processing. To obtain a smooth even contact of the teeth in centric and eccentric positions.

## Slide 6: During flasking and processing changes in the occlusion may occur due to several possible causes called processing errors:
1.Dimensional changes in the wax after setting up of the teeth. This should be very slight if the occlusion of the wax-up was carefully examined before flasking.
2.The heat cured acrylic resin expands and contracts during the curing procedure. It expands as the polymerizing temperature is reached then starts to contract (polymerization shrinkage) .Then as it cools to room temperature it contracts again.
The total effect of this dimensional change is a slight shrinkage which may change the position of the teeth.
3.The expansion of the investing material during the processing.
4.The pressure of the flask press.

## Slide 7: *In order to correct these errors, the dentures are returned to the articulator after deflasking.The casts are repositioned on the original plaster mountings using the key (index) in the base of the cast. The casts are attached to the plaster mountings by sticky wax.
*The condylar elements of the articulator are locked in the centric relation and the articulator is closed. If the incisal pin does not touch the incisal guide table the occlusal vertical dimension has been changed and must be re-established.

## Slide 8: Occlusal adjustment: (Selective grinding)
The sequence of steps should be as follows:
1. Restore the vertical dimension.
2. Refine centric occlusion.
3. Perfect working and balancing occlusion.
4. Correct protrusive occlusion.

## Slide 9: *Selective grinding is carried out using articulating paper to mark the area of premature contacts.
Procedure:
1. Adjust the articulator to the proper setting.
Use red articulating paper for making centric occlusion and blue articulating paper for the eccentric movements.
2. Grind the teeth with small green or diamond stones.

## Slide 10
3. Restore the vertical dimension:
A lateral shift of a tooth or a tooth shifted to produce a high cusp can increase the vertical dimension.
Do not grind the cusp tips unless it is high in every excursion, but rather reduce the fossa or inclined plane of the cusp.
Error: high cusp grind the fossa.
Error: Lateral shift, buccal shift or lingual shift
grind the cusp inclines

## Slide 11: 4.Obtain even contact in centric occlusion:
a. Lock the upper arm of the articulator in centric relation. Check the occlusion by opening and closing the articulator, and lightly tapping the teeth together on red articulating paper.
b. Loosen the locks on the condylar elements and move the denture in eccentric movements.
Using blue articulating paper between the teeth.
- If the cusp is high in centric occlusion only deepen the fossa.
- If the cusp is high in both centric and eccentric position reduce the cusp.

## Slide 12: Reduce the teeth until the incisal pin touches the incisal guide table and uniform contact exists on all posterior teeth. Anterior teeth should not touch in centric occlusion.
5. Adjust the working relation:
Loosen the centric locks and use blue articulating paper.
As a rule in selective grinding the centric holding cusps are not ground. These are : the maxillary lingual cusps and the mandibular buccal cusps.
These cusps are essential to maintain the recorded vertical dimension.
If interferences exists in the working side reduce either the upper buccal cusps or the lower lingual cusps.
This is called B.U.L.L. Rule

## Slide 13: In the bull rule reduce the lingual inclines of the upper buccal cusp and the buccal inclines of the lower lingual cusps.
6. Adjust the balancing relation:
Rule : If interference exists on the balancing side reduce the lingual slope of the lower buccal cusp. The lingual buccal cusp is a centric holding cusp so grind carefully and do not reduce the cusp tip.

## Slide 14: 7. Adjust protrusive relation:
a. If the anterior teeth have heavy contact with no contact on the posterior teeth grind the labial surface of the lower anterior and the palatal surface of the upper anteriors.
b. If heavy posterior contact exists with no anterior contact reduce the distal inclines of the maxillary cusps and the mesial inclines of the mandibular cusps.

## Slide 15: 8. Carborundum paste milling:
The articulator is moved through all the excursive movements using carborundum paste to smooth the various gliding surface of the teeth. Milling must be done lightly to prevent losing balancing contacts which might decrease the vertical dimension.
a. Move the articulator into right lateral, left lateral and protrusive movements.
b. Move the articulator in a circular movement.
Use light strokes do not force or press.

## Slide 16
9. When milling is completed remove all traces of carborundum.
10. The ground surfaces of the teeth must be polished when grinding has been completed.

## Slide 17
Thank you