Experiment No. 7

Standard Test Method for

RESISTANCE TO DEGRADATION OF SMALL-SIZE COARSE AGGREGATE BY ABRASION AND IMPACT IN THE LOS ANGELES MACHINE

(ASTM C131-87)

Purpose:  This test method covers a procedure for testing sizes of coarse aggregate smaller than 1 1/2 in. (37.5 mm) for resistance to degradation using the Los Angeles testing machine.

Apparatus Required:

- Los Angeles Machine - The Los Angeles testing machine, conforming in all its essential characteristics to the design shall be used.

- Sieves

- Balance - A balance or scale accurate within 0.1% of test load over the range required for this test.

- Charge - The charge shall consist of steel spheres averaging approximately 1 27/32 in. (46.8 mm) in diameter and each weighing between 390 and 445 g.  The charge depending upon the grading of the test sample shall be as follows:

| - Grading | - Number of Spheres | - Weight of Charge, g |
| --- | --- | --- |
| - A | - 12 | - 5000  25 |
| - B | - 11 | - 4584  25 |
| - C | - 8 | - 3330  20 |
| - D | - 6 | - 2500  15 |

- Test Sample:

- The test sample washed and oven-dried at 221 to 230 F (105 to 110 C) to substantially constant weight, separated into individual size fractions, and recombined to the grading of Table 9.1.

- Procedure:

- Place the test sample and the charge in the Los Angeles testing machine and rotate the machine at a speed of 30 to 33 rpm for 500 revolutions.  After the prescribed number of revolutions, discharge the material from the machine and make a preliminary separation of the sample on a sieve coarser than the No. 12.

- Sieve the finer portion on No. 12 sieve.  Wash the material coarser than sieve No. 12, oven-dry at 221 to 230 F (105 to 110 C) to substantially constant weight, and weigh to the nearest 1 g.

Experimental Data and Results:

Tabulate the data in the given ‘Test Data Sheet’

TABLE 9.1 Grading of Test Samples

| Sieve Size |  | Weight of Indicated Sizes, g |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Passing Retained on |  | Grading |  |  |  |
|  |  | A | B | C | D |
| 1 1/2 in. | 1 in. | 1 250  25 | - | - | - |
| 1 in. | 3/4 in. | 1 250  25 | - | - | - |
| 3/4 in. | 1/2 in. | 1 250  10 | 2 500  10 | - | - |
| 1/2 in. | 3/8 in. | 1 250  10 | 2 500  10 | - | - |
| 3/8 in. | 1/4 in. | - | - | 2 500  10 | - |
| 1/4 in. | No. 4 | - | - | 2 500  10 | - |
| No. 4 | No. 8 | - | - | - | 5 000  10 |
| Total |  | 5 000  10 | 5 000  10 | 5 000  10 | 5 000  10 |

Calculations:

Express the loss (difference between the original weight and the final weight of the test sample) as a percentage of the original weight of the test sample.  Report this value as the percent loss.

Discussion:  Discuss the following about the test in the given ‘Test Data Sheet’

Experiment No. 9

Test Data Sheet

ABRASION BY LOS ANGELES MACHINE

Sample No. ______________  Description of Material: _________________________________

Tested by: _______________________________  Date of Testing: _______________________

Original Weight of  Sample, g: _________  Charge: ___________ Grading Class: ____________

| Test No. | Weight of Sample Before Test, g | Weight of Sample After Test, g | Percent Loss |
| --- | --- | --- | --- |
| 1 |  |  |  |
| 2 |  |  |  |
| 3 |  |  |  |
| Average Percent Loss |  |  |  |

Discussion of Test Results: _______________________________________________________

_____________________________________________________________________________

_____________________________________________________________________________

_____________________________________________________________________________