Experiment No. 10

Standard Test Method For

SOFTENING POINT OF BITUMEN

(ASTM D 36-86)

Purpose:  This test method covers the determination of softening point of bitumen in range from 30-80 C using the ring-and-ball apparatus immersed in distilled water.

Apparatus Required:

- Rings - Two square-shouldered brass rings conforming to the standard dimensions

- Pouring Plate - A flat, smooth, brass plat approximately 50 by 75 mm  (2 by 3 in.)

- Balls - Tw3o steel balls, 9.5 mm (3/3 in.) in diameter, each having a mass of 3.50  0.05 g.

- Ball-Centering Guides - Two brass guides for centering the steel balls, on for each ring.

- Bath - A glass vessel, capable of being heated, not less than 85 mm in inside diameter and not less than 120 mm in depth from the bottom of the flare.

- Ring Holder and Assembly - A brass holder designed to support the two rings in a horizontal position.

- Thermometers - An ASTM Low Softening Point Thermometer, having a range from -2 to +80 C.

Preparation of Test Specimen:

- Do not start unless it is planned to complete preparation and testing of all asphalt specimens within 6 h.

- Heat bitumen sample with care, stirring frequently to prevent local over heating, until it has become sufficiently fluid to pour.

- Stir carefully to avoid incorporation of air bubbles in the sample.

- Take no more than 2 h to heat an asphalt sample to its pouring temperature; in no case shall this be more than 110 C above the expected softening point of the asphalt.

- Heat the two brass rings (but not the pouring plate) to the approximate pouring temperature, and place them on the pouring plate treated with one of the release agents.

- Pour a slight excess of the heated bitumen into each ring, and then allow the specimens to cool in ambient air for at least 30 min.

- When the specimens have cooled, cut away the excess bitumen cleanly with a slightly heated knife or spatula, so that each disk is flush and level with the top of its ring.

Procedure:

- Take freshly boiled distilled water.  The starting bath temperature shall be 5  1 C.

- Assemble the apparatus with the specimen rings, ball-centering guides, and thermometer in position, and fill the bath so that the liquid depth will be 105  3 mm with the apparatus in place.

- Place the bath in the ice water, and using forceps, place the two steel balls in the bottom of the bath and maintain the starting temperature of 5  1 C for 15 min.

- Again using forceps, place a ball from the bottom of the bath in each ball-centering guide.

- Heat the bath from below so that the temperature indicated by the thermometer rises at a uniform rate of 5 C .  The maximum permissible variation for any 1-min. period after the first 3 min shall be  0.5 C.

- Record for each ring and ball the temperature indicated by the thermometer at the instant the bitumen surrounding the ball touches the bottom plate.

Experimental Data and Results:  Tabulate the data in the given Test Data Sheet.  When using ASTM Thermometer, report to the nearest 0.2 C.

The single-operator standard deviation has been found to be 0.41 C.  Therefore, results of two properly conducted tests by the same operator on the same sample of bitumen should not differ by more than 1.2 C.

Discussion:  Discuss about the results in the given Test Data Sheet.

Experiment No. 12

Test Data Sheet

SOFTENING POINT OF BITUMEN

Sample No.  __________  Description of Material: ____________________________________

Tested by: _______________________________  Date of Testing: _______________________

Test Temperature: ___________ C;   Rate of Heat: ___________ C;

| Ring No. | Instant Temperature, C | Softening Point, Average C |
| --- | --- | --- |
| 1 |  |  |
| 2 |  |  |

| Ring No. | Instant Temperature, C | Softening Point, Average C |
| --- | --- | --- |
| 1 |  |  |
| 2 |  |  |

| Ring No. | Instant Temperature, C | Softening Point, Average C |
| --- | --- | --- |
| 1 |  |  |
| 2 |  |  |

Discussion of Test Results: _______________________________________________________

_____________________________________________________________________________

____________________________________________________________________________