## Slide 1: Out line of lecture
What is superconductivity?
Superconducting materials
Meissner effect
Superconducting parameters
High Tc Superconductors mainly Cuprate
Preparation of HTSC
Structure of Cuprate HTSC

## Slide 2: What is superconductivity?
Disappearance of the electrical resistance of various kind of metals in small temperature range at a critical temperature Tc.
This is the characteristic of certain materials

## Slide 3: Kamerlingh Onnes, awarded 1913 Nobel Prize for Discovery of Superconductivity in Mercury in 1911
Discovery

## Slide 4: Is the resistance identically zero?
How an experiment can show that the resistance is identically zero? All measuring device has limitation to its sensitivity.
An upper limit is 10-27Ω-cm (copper 10-9Ω-cm)

## Slide 5: Superconducting materials
Soon after discovery, various kinds of element tried and found around 26 elements show superconductivity.
Among elements Maximum Tc 9.26 K in Nb and lowest 0.012K in Tungsten
Tc depends not only chemical composition but also crystal structure. -La and -La have Tc 4.9K and 6.06K.
This means the superconductivity is not a property of isolated atoms but it is collective effect determined by the structure of the whole samples

## Slide 6: Superconducting materials
It was expected that the good conductor mainly copper silver and gold may turn to superconductivity at low temperature but they did not.
Majority of superconductors are not pure element, but alloys and compound. Today over 6000 SCs are known and are constantly growing.

## Slide 7: Superconducting materials
For many years the record holder for maximum Tc was Niobium-tin alloy (18.1K) and in 1973 discovered 22.3 K in thin film of Nb3Ge.
In 1986, 75 th anniversary of discovery of superconductivity was marked by new class of superconductors copper oxide based.

## Slide 8: Superconducting materials
A. Bednorz and K.A. Muller (IBM Zurich) discovered La-Ba-Cu-O system with 30K Tc
What made this discovery so remarkable was that ceramics are normally insulators. They don't conduct electricity well at all. So, researchers had not considered them as possible high-temperature superconductor candidates.
This discovary won the Noble prize in 1987

## Slide 9: Superconducting materials
Müller and Bednorz' discovery triggered a flurry of activity in the field of superconductivity.
Researchers around the world began "cooking" up ceramics of every imaginable combination in a quest for higher and higher Tc's.
In January of 1987 a research team at the University of Alabama-Huntsville substituted Yttrium for Lanthanum in the Müller and Bednorz molecule and achieved an incredible 92 K Tc.
For the first time a material (today referred to as YBCO) had been found that would superconduct at temperatures warmer than liquid nitrogen - a commonly available coolant.

## Slide 10: Perfect diamagnetism Meissner effect
The next hall mark to be discovered was the perfect diamagnetism, in 1933 by Meissner and Oschenfield
An unintuitive (un-imaginable)
property of superconductors

## Slide 11: Meissner effect
A diamagnetic property exhibited by superconductors.
End result is the exclusion of magnetic field from the interior of a superconductor.
What is diamagnetism?

## Slide 12: Diamagnetism?
A superconductor is not only a perfect conductor (R=0), but a perfect diamagnet.
It will tend to repel a magnet.

## Slide 13: So, Superconductors are Perfect Diamagnets?
If a superconductor was only a perfect conductor, would there be a Meissner Effect?
Notes: <number>

## Slide 14: A “perfect conductor”
Field cooled
BA
BA
cool
Remove
BA
BA
Zero field cooled
BA=0
BA=0
cool
Apply
BA
Remove
BA

## Slide 15: A superconductor - cooled in zero field
BA=0
Apply
BA
dB/dt must be zero in a closed resistanceless loop so screening currents flow to generate a field equal and opposite to BA within the superconductor
Remove
BA
As BA is reduced to zero, dB/dt must remain at zero, so the screening currents also decrease to zero.
cool
BA=0
The superconductor is cooled in zero magnetic flux density to below “Tc”
Precisely the same as a perfect conductor

## Slide 16: superconductor perfect conductor
Zero field cooled
BA=0
BA=0
cool
Apply
BA
Remove
BA
BA=0
BA=0
cool
Apply
BA
Remove
BA
Zero field cooled

## Slide 17: A superconductor” - cooled in a field
BA
A magnetic flux density BA is applied to the superconductor at high temperatures
This is the Meissner Effect - it shows that not only must dB/dt=0 within a superconductor - but B itself must remain zero
cool
It is then cooled in a magnetic flux density BA to below “Tc”
BA
Remove
BA
As the applied magnetic flux density is reduced to zero, the screening currents also decrease to ensure that dB/dt=0 within the superconductor.
BA
All magnetic flux is spontaneously excluded from the body of the superconductor - even though the applied flux density is unchanged and dB/dt=0 . Screening currents must therefore begin flow in a time invariant field to produce fields equal and opposite to BA!!

## Slide 18: perfect conductor superconductor
Field cooled
BA
cool
Remove
BA
BA
Apply
BA
BA
BA
cool
Remove
BA
BA
Field cooled

## Slide 19: Net flux distribution - solid sample
applied flux
flux from magnetisation
screening currents
An example of perfect diamagnetism

## Slide 20: The Meissner Effect - summary
Between 1911 and 1933 researchers considered that a superconductor was no more than a resistanceless perfect conductor
By measuring the properties of a superconductor cooled in a magnetic field they showed that not only
dB/dt=0 but also B=0.
The ability of a superconductor to expel magnetic flux from its interior is the Meissner Effect
It is the first indication that the superconducting state is an entirely new state of matter
It shows that in a superconductor currents can be induced to flow in a time invariant field - in violation of Maxwell’s equations
Summary: Superconductors expel all magnetic flux and exhibit zero resistance
Notes: <number>
Show how it violates Maxwell's equation see notes…I.e assume r=0 does not explain superconductivty fully!

## Slide 21: Critical field
Meissner effect implies that the superconductivity will be destroyed by critical magnetic field HC which is related thermodynamically to the free enrgy
Temperature depenedence is given by
Phase transition in zero field at Tcis of 2nd order while in magnetic field is of first order

## Slide 22: Type I and Type II superconductors
Superconductors exist in one of two types. In the first kind an external magnetic field cannot penetrate into the bulk of the sample without destroying the superconducting condensate state that is called Type I or Soft superconductors.
The second kind of superconductors, of which HTS are prominent members, are able to remain superconducting over a range of fields H in the interval Hc1 < H < Hc2. At the lower critical field Hc1 the first magnetic flux starts to enter the bulk of the superconductor. The field does not penetrate the bulk in a homogenous way rather in a regular array of flux tubes each carrying one quantum of flux o = 2.07x10-7 G-cm2

## Slide 23: The magnetisation of a type II superconductor as function of the applied magnetic field

## Slide 24: Vortices!

## Slide 25: An illustration of a vortex line and the important lengths, the penetration depth and the coherence length

## Slide 26: Mystery of Superconductivity
Isotope Effect: Probably this is the effect, which shows the way to the correct theory.
TC M1/2 = constant
Isotope mass is the characteristic of lattice and related to the lattice vibration Ω≈M-0.5. Superconductivity is the property of electron system. Thus this means the electron lattice interaction is related to superconductivity.
Also the lattice interaction is responsible for electrical resistance.

## Slide 27: Mystery of Superconductivity
The first widely-accepted theory in understanding of superconductivity was given in 1957 by John Bardeen, Leon Cooper, and John Schrieffer. Their Theories of Superconductivity became known as the BCS theory - and won them a Nobel prize in 1972.

## Slide 28: BCS Theory
The two electrons forms a pair i.e. called Cooper pair. This pair is no more fermion rather, it is boson and follow Bose Einstein statistics.
The lattice play a role in providing the attraction between the two electrons
An electron moving in the metal deform lattice or polarize it and electron surrounded by the cloud of positive charge attract the other electron.

## Slide 29: High Tc Superconductors
Müller and Bednorz' discovery of La-Ba-Cu-O around 30K triggered a flurry of activity in the field of superconductivity.
Researchers around the world began "cooking" up ceramics of every imaginable combination in a quest for higher and higher Tc's.
In January of 1987 a research team at the University of Alabama-Huntsville substituted Yttrium for Lanthanum in the Müller and Bednorz molecule and achieved an incredible 92 K Tc. For the first time a material YBa2Cu3O7-(today referred to as YBCO or 123) had been found that would superconduct at temperatures warmer than liquid nitrogen - a commonly available coolant.

## Slide 30: Preperation of YBa2Cu3O7- superconductors by solid state reaction
Y2O3, BaCO3 and CuO are mixed in Stoichiometric
Powder were calcined and mixed twice or thrice at 950C for 4 to 5 hours
Pressed in pellet and sintered at 950C (heat just below the melting point to increase strength and density and to promote intergranular bonding) for 12 to 24 hours.
Allow the furnace to cool to 500-600°C for the crucial "sensitization" step. Flow Oxygen for three hours and cool slowly from 600 to 400C
Several annealing procedures, heating and cooling cycles, seem to improve the quality of 1-2-3 ceramic superconductors.

## Slide 31: Variation of TC with Oxygen content

## Slide 32: Two types of Cu site Layers of CuO5 square pyramids (elongation essentially vertex-linked CuO4 squares again) Chains of vertex-linked CuO4 squares

## Slide 33: High Tc Superconductors
The French group under Bernard Raveau, soon announced the existence of another new type of superconductor, based on the substitution of bismuth for lanthanum in La-Sr-Cu-O. This new superconductor (“Bi2Sr2CuO6”),which was found to have a crystal structure different from 123 and the K2NiF4 materials, ultimately turned out to be the first of a gigantic class of new materials to follow. Its Tc was ,10 K.
T Maeda from NIRM, Tsukuba add Ca and increased TC greater than 80 K,

## Slide 34: Bi2Sr2CaCu2O8 (2212)
The crystal structure of the 80 K superconductor in theBi-Sr-Ca-Cu-O system is shown in Fig formula is Bi2Sr2CaCu2O8.
There are no copper oxide chains and, therefore, that ended all discussion aboutwhether those chains could be the reason for the high Tc in the 123compound. What this does have in common with the 123 compoundis a double layer of CuO2 planes.

## Slide 35: Tc depending on no. of CuO2 layer and the Insulating layer
Bi2Sr2Ca2Cu3O10 (2223) – 110 K
Tl2Ba2Ca2Cu3O10 - 125K
HgBa2Ca2Cu3O9, - 134K at high pressure164 K
Y2Ba4Cu7O15 Tc~95K

## Slide 36: Large Scale Applications
Top speed: 552 km/hr
In-place in Detroit.*
US Navy: 5,000 HP*
*American Superconductor Corp.

## Slide 37: Conclusion
New Materials are coming showing higher and higher Tc
Next challenge is to make the materials suitable for application
Dreamed room temperature superconductors may be reality one day