## Slide 1: CHAPTER OBJECTIVES
Show relationship of stress and strain using experimental methods to determine stress-strain diagram of a specific material
Discuss the behavior described in the diagram for commonly used engineering materials
Discuss the mechanical properties and other test related to the development of mechanics of materials

## Slide 2: CHAPTER OUTLINE
Tension and Compression Test
Stress-Strain Diagram
Stress-Strain Behavior of Ductile and Brittle Materials
Hooke’s Law
Strain Energy
Poission’s Ratio
Shear Stress-Strain Diagram
*Failure of Materials Due to Creep and Fatigue

## Slide 3: 3.1 TENSION & COMPRESSION TEST
Strength of a material can only be determined by experiment
One test used by engineers is the tension or compression test
This test is used primarily to determine the relationship between the average normal stress and average normal strain in common engineering materials, such as metals, ceramics, polymers and composites

## Slide 4: 3.1 TENSION & COMPRESSION TEST
Performing the tension or compression test
Specimen of material is made into “standard” shape and size
Before testing, 2 small punch marks identified along specimen’s length
Measurements are taken of both specimen’s initial x-sectional area A0 and gauge-length distance L0; between the two marks
Seat the specimen into a testing machine shown below

## Slide 5: 3.1 TENSION & COMPRESSION TEST
Performing the tension or compression test
Seat the specimen into a testing machine shown below
The machine will stretch specimen at slow constant rate until breaking point
At frequent intervals during test, data is recorded of the applied load P.

## Slide 6: 3.1 TENSION & COMPRESSION TEST
Performing the tension or compression test
Elongation δ = L − L0 is measured using either a caliper or an extensometer
δ is used to calculate the normal strain in the specimen
Sometimes, strain can also be read directly using an electrical-resistance strain gauge

## Slide 7: 3.2 STRESS-STRAIN DIAGRAM
A stress-strain diagram is obtained by plotting the various values of the stress and corresponding strain in the specimen
Conventional stress-strain diagram
Using recorded data, we can determine nominal or engineering stress by
P
A0
σ =
Assumption: Stress is constant over the x-section and throughout region between gauge points

## Slide 8: 3.2 STRESS-STRAIN DIAGRAM
Conventional Stress-Strain Diagram
Likewise, nominal or engineering strain is found directly from strain gauge reading, or by
δ
L0
 =
Assumption: Strain is constant throughout region between gauge points
By plotting σ (ordinate) against  (abscissa), we get a conventional stress-strain diagram

## Slide 9: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure shows the characteristic stress-strain diagram for steel, a commonly used material for structural members and mechanical elements

## Slide 10: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Elastic behavior.
A straight line
Stress is proportional to strain, i.e., linearly elastic
Upper stress limit, or proportional limit; σpl
If load is removed upon reaching elastic limit, specimen will return to its original shape

## Slide 11: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure 3-4
Yielding.
Material deforms permanently; yielding; plastic deformation
Yield stress, σY
Once yield point reached, specimen continues to elongate (strain) without any increase in load
Note figure not drawn to scale, otherwise induced strains is 10-40 times larger than in elastic limit
Material is referred to as being perfectly plastic

## Slide 12: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure 3-4
Strain hardening.
Ultimate stress, σu
While specimen is elongating, its x-sectional area will decrease
Decrease in area is fairly uniform over entire gauge length

## Slide 13: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure 3-4
Necking.
At ultimate stress, x-sectional area begins to decrease in a localized region
As a result, a constriction or “neck” tends to form in this region as specimen elongates further
Specimen finally breaks at fracture stress, σf

## Slide 14: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure 3-4
Necking.
Specimen finally breaks at fracture stress, σf

## Slide 15: 3.2 STRESS-STRAIN DIAGRAM
True stress-strain diagram
Instead of using original cross-sectional area and length, we can use the actual cross-sectional area and length at the instant the load is measured
Values of stress and strain thus calculated are called true stress and true strain, and a plot of their values is the true stress-strain diagram

## Slide 16: 3.2 STRESS-STRAIN DIAGRAM
True stress-strain diagram
In strain-hardening range, conventional σ- diagram shows specimen supporting decreasing load
While true σ- diagram shows material to be sustaining increasing stress

## Slide 17: 3.2 STRESS-STRAIN DIAGRAM
True stress-strain diagram
Although both diagrams are different, most engineering design is done within elastic range provided
  Material is “stiff,” like most metals
  Strain to elastic limit remains small
  Error in using engineering values of σ and  is very small (0.1 %) compared to true values

## Slide 18: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Ductile materials
Defined as any material that can be subjected to large strains before it ruptures, e.g., mild steel
Such materials are used because it is capable of absorbing shock or energy, and if before becoming overloaded, will exhibit large deformation before failing
Ductility of material is to report its percent elongation or percent reduction in area at time of fracture

## Slide 19: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Ductile materials
Percent elongation is the specimen’s fracture strain expressed as a percent
Percent reduction in area is defined within necking region as
Percent elongation =
Lf − L0
L0
(100%)
Percent reduction in area =
A0 − Af
A0
(100%)

## Slide 20: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Ductile materials
Most metals do not exhibit constant yielding behavior beyond the elastic range, e.g. aluminum
It does not have well-defined yield point, thus it is standard practice to define its yield strength using a graphical procedure called the offset method

## Slide 21: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Ductile materials
Offset method to determine yield strength
Normally, a 0.2 % strain is chosen.
From this point on the  axis, a line parallel to initial straight-line portion of stress-strain diagram is drawn.
The point where this line intersects the curve defines the yield strength.

## Slide 22: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Brittle Materials
Material that exhibit little or no yielding before failure are referred to as brittle materials, e.g., gray cast iron
Brittle materials do not have a well-defined tensile fracture stress, since appearance of initial cracks in a specimen is quite random

## Slide 23: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Brittle Materials
Instead, the average fracture stress from a set of observed tests is generally reported

## Slide 24: 3.4 HOOKE’S LAW
E represents the constant of proportionality, also called the modulus of elasticity or Young’s modulus
E has units of stress, i.e., pascals, MPa or GPa.
Most engineering materials exhibit a linear relationship between stress and strain with the elastic region
Discovered by Robert Hooke in 1676 using springs, known as Hooke’s law
σ = E

## Slide 25: 3.4 HOOKE’S LAW
As shown above, most grades of steel have same modulus of elasticity, Est = 200 GPa
Modulus of elasticity is a mechanical property that indicates the stiffness of a material
Materials that are still have large E values, while spongy materials (vulcanized rubber) have low values

## Slide 26: 3.4 HOOKE’S LAW
IMPORTANT
Modulus of elasticity E, can be used only if a material has linear-elastic behavior.
Also, if stress in material is greater than the proportional limit, the stress-strain diagram ceases to be a straight line and the equation is not valid

## Slide 27: 3.4 HOOKE’S LAW
Strain hardening
If a specimen of ductile material (steel) is loaded into the plastic region and then unloaded, elastic strain is recovered as material returns to its equilibrium state
However, plastic strain remains, thus material is subjected to a permanent set

## Slide 28: 3.4 HOOKE’S LAW
Strain hardening
Specimen loaded beyond yield point A to A’
Inter-atomic forces have to be overcome to elongate specimen elastically, these same forces pull atoms back together when load is removed
Since E is the same, slope of line O’A’ is the same as line OA

## Slide 29: 3.4 HOOKE’S LAW
Strain hardening
Load reapplied, atoms will be displaced until yielding occurs at or near A’, and stress-strain diagram continues along same path as before
New stress-strain diagram has higher yield point (A’), a result of strain-hardening
Specimen has a greater elastic region and less ductility

## Slide 30: 3.4 HOOKE’S LAW
Strain hardening
As specimen is unloaded and loaded, heat or energy may be lost
Colored area between the curves represents lost energy and is called mechanical hysteresis
It’s an important consideration when selecting materials to serve as dampers for vibrating structures and equipment