## Slide 1: 3.5 STRAIN ENERGY
When material is deformed by external loading, energy is stored internally throughout its volume
Internal energy is also referred to as strain energy
Stress develops a force,
F = σ A = σ (x y)

## Slide 2: 3.5 STRAIN ENERGY
Strain-energy density is strain energy per unit volume of material
u =
∆U
∆V
σ
2
=
If material behavior is linear elastic, Hooke’s law applies,
u =
σ
2
σ2
2E
=
σ

( )

## Slide 3: 3.5 STRAIN ENERGY
Modulus of resilience
When stress reaches proportional limit, strain-energy-energy density is called modulus of resilience
A material’s resilience represents its ability to absorb energy without any permanent damage
ur =
σpl pl
2
σpl2
2E
=

## Slide 4: 3.5 STRAIN ENERGY
Modulus of toughness
Modulus of toughness ut, indicates the strain-energy density of material before it fractures
Shaded area under stress-strain diagram is the modulus of toughness
Used for designing members that may be accidentally overloaded
Higher ut is preferable as distortion is noticeable before failure

## Slide 5: EXAMPLE 3.1
Tension test for a steel alloy results in the stress-strain diagram below.
Calculate the modulus of elasticity and the yield strength based on a 0.2%.

## Slide 6
Modulus of elasticity
Calculate the slope of initial straight-line portion of the graph. Use magnified curve and scale shown in light blue, line extends from O to A, with coordinates (0.0016 mm, 345 MPa)
E =
345 MPa
0.0016 mm/mm
= 215 GPa
EXAMPLE 3.1 (SOLN)

## Slide 7
Yield strength
At 0.2% strain, extrapolate line (dashed) parallel to OA till it intersects stress-strain curve at A’
σYS = 469 MPa
EXAMPLE 3.1 (SOLN)

## Slide 8
Ultimate stress
Defined at peak of graph, point B,
σu = 745.2 MPa
EXAMPLE 3.1 (SOLN)

## Slide 9
Fracture stress
When specimen strained to maximum of f = 0.23 mm/mm, fractures occur at C.
Thus,
σf = 621 MPa
EXAMPLE 3.1 (SOLN)

## Slide 10: 3.6 POISSON’S RATIO
When body subjected to axial tensile force, it elongates and contracts laterally
Similarly, it will contract and its sides expand laterally when subjected to an axial compressive force

## Slide 11: 3.6 POISSON’S RATIO
Strains of the bar are:
long =
δ
L
lat =
δ’
r
Poisson’s ratio, ν = −
lat
long
Early 1800s, S.D. Poisson realized that within elastic range, ration of the two strains is a constant value, since both are proportional.

## Slide 12: 3.6 POISSON’S RATIO
ν is unique for homogenous and isotropic material
Why negative sign? Longitudinal elongation cause lateral contraction (-ve strain) and vice versa
Lateral strain is the same in all lateral (radial) directions
Poisson’s ratio is dimensionless, 0 ≤ ν ≤ 0.5

## Slide 13: EXAMPLE 3.4
Bar is made of A-36 steel and behaves elastically.
Determine change in its length and change in dimensions of its cross section after load is applied.

## Slide 14: EXAMPLE 3.4 (SOLN)
Normal stress in the bar is
σz =
P
A
= 16.0(106) Pa
From tables, Est = 200 GPa, strain in z-direction is
z =
σz
Est
= 80(10−6) mm/mm
Axial elongation of the bar is,
δz = zLz = [80(10−6)](1.5 m) = −25.6 μm/m

## Slide 15: EXAMPLE 3.4 (SOLN)
Using νst = 0.32, contraction strains in both x and y directions are
Thus changes in dimensions of cross-section are
x = y = −νstz = −0.32[80(10−6)] = −25.6 μm/m
δx = xLx = −[25.6(10−6)](0.1 m) = −25.6 μm
δy = yLy = −[25.6(10−6)](0.05 m) = −1.28 μm

## Slide 16: 3.6 SHEAR STRESS-STRAIN DIAGRAM
Use thin-tube specimens and subject it to torsional loading
Record measurements of applied torque and resulting angle of twist

## Slide 17: 3.6 SHEAR STRESS-STRAIN DIAGRAM
Material will exhibit linear-elastic behavior till its proportional limit, τpl
Strain-hardening continues till it reaches ultimate shear stress, τu
Material loses shear strength till it fractures, at stress of τf

## Slide 18: 3.6 SHEAR STRESS-STRAIN DIAGRAM
Hooke’s law for shear
τ = Gγ
G is shear modulus of elasticity or modulus of rigidity
G can be measured as slope of line on τ-γ diagram, G = τpl/ γpl
The three material constants E, ν, and G is related by
G =
E
2(1 + ν)

## Slide 19: EXAMPLE 3.5
Specimen of titanium alloy tested in torsion & shear stress-strain diagram shown below.
Determine shear modulus G, proportional limit, and ultimate shear stress.
Also, determine the maximum distance d that the top of the block shown, could be displaced horizontally if material behaves elastically when acted upon by V. Find magnitude of V necessary to cause this displacement.

## Slide 20: EXAMPLE 3.5 (SOLN)
Shear modulus
Obtained from the slope of the straight-line portion OA of the τ-γ diagram. Coordinates of A are (0.008 rad, 360 MPa)
G =
= 45(103) MPa
360 MPa
0.008 rad

## Slide 21: EXAMPLE 3.5 (SOLN)
Proportional limit
By inspection, graph ceases to be linear at point A, thus,
τpl = 360 MPa
Ultimate stress
From graph,
τu = 504 MPa

## Slide 22: EXAMPLE 3.5 (SOLN)
Maximum elastic displacement and shear force
By inspection, graph ceases to be linear at point A, thus,
tan (0.008 rad) ≈ 0.008 rad =
d
50 mm
d = 0.4 mm
τavg =
V
A
360 MPa =
V
(75 mm)(100 mm)
V = 2700 kN

## Slide 23: *3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Creep
Occurs when material supports a load for very long period of time, and continues to deform until a sudden fracture or usefulness is impaired
Is only considered when metals and ceramics are used for structural members or mechanical parts subjected to high temperatures
Other materials (such as polymers & composites) are also affected by creep without influence of temperature

## Slide 24: *3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Creep
Stress and/or temperature significantly affects the rate of creep of a material
Creep strength represents the highest initial stress the material can withstand during given time without causing specified creep strain
Simple method to determine creep strength
Test several specimens simultaneously
  At constant temperature, but
  Each specimen subjected to different axial stress

## Slide 25: *3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Creep
Simple method to determine creep strength
Measure time taken to produce allowable strain or rupture strain for each specimen
Plot stress vs. strain
Creep strength inversely proportional to temperature and applied stresses

## Slide 26: *3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Fatigue
Defined as a metal subjected to repeated cycles of stress and strain, breaking down structurally, before fracturing
Needs to be accounted for in design of connecting rods (e.g. steam/gas turbine blades, connections/supports for bridges, railroad wheels/axles and parts subjected to cyclic loading)
Fatigue occurs at a stress lesser than the material’s yield stress

## Slide 27: *3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Fatigue
Also referred to as the endurance or fatigue limit
Method to get value of fatigue
Subject series of specimens to specified stress and cycled to failure
Plot stress (S) against number of cycles-to-failure N (S-N diagram) on logarithmic scale

## Slide 28: CHAPTER REVIEW
Tension test is the most important test for determining material strengths. Results of normal stress and normal strain can then be plotted.
Many engineering materials behave in a linear-elastic manner, where stress is proportional to strain, defined by Hooke’s law, σ = E. E is the modulus of elasticity, and is measured from slope of a stress-strain diagram
When material stressed beyond yield point, permanent deformation will occur.

## Slide 29: CHAPTER REVIEW
Strain hardening causes further yielding of material with increasing stress
At ultimate stress, localized region on specimen begin to constrict, and starts “necking”. Fracture occurs.
Ductile materials exhibit both plastic and elastic behavior. Ductility specified by permanent elongation to failure or by the permanent reduction in cross-sectional area
Brittle materials exhibit little or no yielding before failure

## Slide 30: CHAPTER REVIEW
Yield point for material can be increased by strain hardening, by applying load great enough to cause increase in stress causing yielding, then releasing the load. The larger stress produced becomes the new yield point for the material
Deformations of material under load causes strain energy to be stored. Strain energy per unit volume/strain energy density is equivalent to area under stress-strain curve.

## Slide 31: CHAPTER REVIEW
The area up to the yield point of stress-strain diagram is referred to as the modulus of resilience
The entire area under the stress-strain diagram is referred to as the modulus of toughness
Poisson’s ratio (ν), a dimensionless property that measures the lateral strain to the longitudinal strain [0 ≤ ν ≤ 0.5]
For shear stress vs. strain diagram: within elastic region, τ = Gγ, where G is the shearing modulus, found from the slope of the line within elastic region

## Slide 32: CHAPTER REVIEW
G can also be obtained from the relationship of G = E/[2(1+ ν)]
When materials are in service for long periods of time, creep and fatigue are important.
Creep is the time rate of deformation, which occurs at high stress and/or high temperature. Design the material not to exceed a predetermined stress called the creep strength

## Slide 33: CHAPTER REVIEW
Fatigue occur when material undergoes a large number of cycles of loading. Will cause micro-cracks to occur and lead to brittle failure.
Stress in material must not exceed specified endurance or fatigue limit