## Slide 1: 4.5 FORCE METHOD OF ANALYSIS FOR AXIALLY LOADED MEMBERS
Used to also solve statically indeterminate problems by using superposition of the forces acting on the free-body diagram
First, choose any one of the two supports as “redundant” and remove its effect on the bar
Thus, the bar becomes statically determinate
Apply principle of superposition and solve the equations simultaneously

## Slide 2: 4.5 FORCE METHOD OF ANALYSIS FOR AXIALLY LOADED MEMBERS
From free-body diagram, we can determine the reaction at A
+
=

## Slide 3: 4.5 FORCE METHOD OF ANALYSIS FOR AXIALLY LOADED MEMBERS
Procedure for Analysis
Compatibility
Choose one of the supports as redundant and write the equation of compatibility.
Known displacement at redundant support (usually zero), equated to displacement at support caused only by external loads acting on the member plus the displacement at the support caused only by the redundant reaction acting on the member.

## Slide 4: 4.5 FORCE METHOD OF ANALYSIS FOR AXIALLY LOADED MEMBERS
Procedure for Analysis
Compatibility
Express external load and redundant displacements in terms of the loadings using load-displacement relationship
Use compatibility equation to solve for magnitude of redundant force

## Slide 5: 4.5 FORCE METHOD OF ANALYSIS FOR AXIALLY LOADED MEMBERS
Procedure for Analysis
Equilibrium
Draw a free-body diagram and write appropriate equations of equilibrium for member using calculated result for redundant force.
Solve the equations for other reactions

## Slide 6: EXAMPLE 4.9
A-36 steel rod shown has diameter of 5 mm. It’s attached to fixed wall at A, and before it is loaded, there’s a gap between wall at B’ and rod of 1 mm.
Determine reactions at A and B’.

## Slide 7: EXAMPLE 4.9 (SOLN)
Compatibility
Consider support at B’ as redundant.
Use principle of superposition,
0.001 m = δP −δB Equation 1
( + )

## Slide 8: EXAMPLE 4.9 (SOLN)
Compatibility
Deflections δP and δB are determined from Eqn. 4-2
δP =
PLAC
AE
= … = 0.002037 m
δB =
FB LAB
AE
= … = 0.3056(10-6)FB
Substituting into Equation 1, we get
0.001 m = 0.002037 m − 0.3056(10-6)FB
FB = 3.40(103) N = 3.40 kN

## Slide 9: EXAMPLE 4.9 (SOLN)
Equilibrium
From free-body diagram
− FA + 20 kN − 3.40 kN = 0
FA = 16.6 kN
+ Fx = 0;

## Slide 10: 4.6 THERMAL STRESS
Expansion or contraction of material is linearly related to temperature increase or decrease that occurs (for homogenous and isotropic material)
From experiment, deformation of a member having length L is
δT = α ∆T L
α = liner coefficient of thermal expansion. Unit measure strain per degree of temperature: 1/oC (Celsius) or 1/oK (Kelvin)
∆T = algebraic change in temperature of member
δT = algebraic change in length of member

## Slide 11: 4.6 THERMAL STRESS
For a statically indeterminate member, the thermal displacements can be constrained by the supports, producing thermal stresses that must be considered in design.

## Slide 12: EXAMPLE 4.10
A-36 steel bar shown is constrained to just fit between two fixed supports when T1 = 30oC.
If temperature is raised to T2 = 60oC, determine the average normal thermal stress developed in the bar.

## Slide 13: EXAMPLE 4.10 (SOLN)
Equilibrium
As shown in free-body diagram,
FA = FB = F
+↑  Fy = 0;
Problem is statically indeterminate since the force cannot be determined from equilibrium.
Compatibility
Since δA/B =0, thermal displacement δT at A occur. Thus compatibility condition at A becomes
+↑
δA/B = 0 = δT − δF

## Slide 14: EXAMPLE 4.10 (SOLN)
From magnitude of F, it’s clear that changes in temperature causes large reaction forces in statically indeterminate members.
Average normal compressive stress is
Compatibility
Apply thermal and load-displacement relationship,
0 = α ∆TL −
FL
AL
F = α ∆TAE = … = 7.2 kN
F
A
σ =
= … = 72 MPa

## Slide 15: 4.7 STRESS CONCENTRATIONS
Force equilibrium requires magnitude of resultant force developed by the stress distribution to be equal to P. In other words,
This integral represents graphically the volume under each of the stress-distribution diagrams shown.
P = ∫A σ dA

## Slide 16: 4.7 STRESS CONCENTRATIONS
In engineering practice, actual stress distribution not needed, only maximum stress at these sections must be known. Member is designed to resist this stress when axial load P is applied.
K is defined as a ratio of the maximum stress to the average stress acting at the smallest cross section:
K =
σmax
σavg
Equation 4-7

## Slide 17: 4.7 STRESS CONCENTRATIONS
K is independent of the bar’s geometry and the type of discontinuity, only on the bar’s geometry and the type of discontinuity.
As size r of the discontinuity is decreased, stress concentration is increased.
It is important to use stress-concentration factors in design when using brittle materials, but not necessary for ductile materials
Stress concentrations also cause failure structural members or mechanical elements subjected to fatigue loadings

## Slide 18: EXAMPLE 4.13
Steel bar shown below has allowable stress,
σallow = 115 MPa. Determine largest axial force P that the bar can carry.

## Slide 19: EXAMPLE 4.13 (SOLN)
Because there is a shoulder fillet, stress-concentrating factor determined using the graph below

## Slide 20: EXAMPLE 4.13 (SOLN)
Calculating the necessary geometric parameters yields
Thus, from the graph, K = 1.4
Average normal stress at smallest x-section,
r
n
=
10 mm
20 mm
= 0.50
w
h
40 mm
20 mm
= 2
=
P
(20 mm)(10 mm)
σavg =
= 0.005P N/mm2

## Slide 21: EXAMPLE 4.13 (SOLN)
Applying Eqn 4-7 with σallow = σmax yields
σallow = K σmax
115 N/mm2 = 1.4(0.005P)
P = 16.43(103) N = 16.43 kN

## Slide 22: *4.8 INELASTIC AXIAL DEFORMATION
Sometimes, a member is designed so that the loading causes the material to yield and thereby permanently deform.
Such members are made from highly ductile material such as annealed low-carbon steel having a stress-strain diagram shown below.
Such material is referred to as being elastic perfectly plastic or elastoplastic

## Slide 23: *4.8 INELASTIC AXIAL DEFORMATION
Plastic load PP is the maximum load that an elastoplastic member can support

## Slide 24: EXAMPLE 4.16
Steel bar shown assumed to be elastic perfectly plastic with σY = 250 MPa.
Determine (a) maximum value of applied load P that can be applied without causing the steel to yield, (b) the maximum value of P that bar can support. Sketch the stress distribution at the critical section for each case.

## Slide 25: EXAMPLE 4.16 (SOLN)
(a) When material behaves elastically, we must use a stress-concentration that is unique for the bar’s geometry.
r
n
=
4 mm
(40 mm − 8 mm)
= 0.125
w
h
40 mm
(40 mm − 8 mm)
= 1.25
=
When σmax = σY. Average normal stress is σavg = P/A
σmax = K σavg;
PY
A
σY = K
( )
…
PY = 16.0 kN

## Slide 26: EXAMPLE 4.16 (SOLN)
Load PY was calculated using the smallest x-section. Resulting stress distribution is shown. For equilibrium, the “volume” contained within this distribution must equal 9.14 kN.

## Slide 27: EXAMPLE 4.16 (SOLN)
Maximum load sustained by the bar causes all material at smallest x-section to yield. As P is increased to plastic load PP, the stress distribution changes as shown.
When σmax = σY. Average normal stress is σavg = P/A
σmax = K σavg;
PY
A
σY = K
( )
…
PP = 16.0 kN
Here, PP equals the “volume” contained within the stress distribution, i.e., PP = σY A

## Slide 28: *4.9 RESIDUAL STRESS
For axially loaded member or group of such members, that form a statically indeterminate system that can support both tensile and compressive loads,
Then, excessive external loadings which cause yielding of the material, creates residual stresses in the members when loads are removed.
Reason is the elastic recovery of the material during unloading

## Slide 29: *4.9 RESIDUAL STRESS
To solve such problem, complete cycle of loading and unloading of member is considered as the superposition of a positive load (loading) on a negative load (unloading).
Loading (OC) results in a plastic stress distribution
Unloading (CD) results only in elastic stress distribution
Superposition requires loads to cancel, however, stress distributions will not cancel, thus residual stresses remain

## Slide 30: EXAMPLE 4.17
Steel rod has radius of 5 mm, made from an elastic-perfectly plastic material for which σY = 420 MPa, E = 70 GPa.
If P = 60 kN applied to rod and then removed, determine residual stress in rod and permanent displacement of collar at C.

## Slide 31: EXAMPLE 4.17 (SOLN)
By inspection, rod statically indeterminate.
An elastic analysis (discussed in 4.4) produces:
FA = 45 kN FB = 15 kN
Thus, this result in stress of
σAC =
45 kN
(0.005 m)2
= 573 MPa (compression) > σY = 420 MPa
σCB =
15 kN
(0.005 m)2
= 191 MPa
And

## Slide 32: EXAMPLE 4.17 (SOLN)
Since AC will yield, assume AC become plastic, while CB remains elastic
(FA)Y = σY A = ... = 33.0 kN
Thus, FB = 60 kN  33.0 kN = 27.0 kN
σAC = σY = 420 MPa (compression)
σCB =
27 kN
(0.005 m)2
= 344 MPa (tension) < 420 MPa (OK!)

## Slide 33: EXAMPLE 4.17 (SOLN)
Residual Stress.
Since CB responds elastically,
Thus,
CB = C / LCB
= +0.004913
C =
FB LCB
AE
= ... = 0.001474 m
AC = C / LAC
= 0.01474

## Slide 34: EXAMPLE 4.17 (SOLN)
Residual Stress.
(σAC)r = 420 MPa + 573 MPa = 153 MPa
(σCB)r = 344 MPa  191 MPa = 153 MPa
Both tensile stress is the same, which is to be expected.

## Slide 35: EXAMPLE 4.17 (SOLN)
Permanent Displacement
Residual strain in CB is
’CB = /E = ... = 0.0022185
C = ’CB LCB = 0.002185(300 mm) = 0.656 mm
So permanent displacement of C is
Alternative solution is to determine residual strain ’AC, and ’AC = AC + AC and
C = ’AC LAC = ... = 0.656 mm

## Slide 36: CHAPTER REVIEW
When load applied on a body, a stress distribution is created within the body that becomes more uniformly distributed at regions farther from point of application. This is the Saint-Venant’s principle.
Relative displacement at end of axially loaded member relative to other end is determined from
If series of constant external forces are applied and AE is constant, then
δ =
∫0
P(x) dx
A(x) E
L
δ =
PL
AE


## Slide 37: CHAPTER REVIEW
Make sure to use sign convention for internal load P and that material does not yield, but remains linear elastic
Superposition of load & displacement is possible provided material remains linear elastic and no changes in geometry occur
Reactions on statically indeterminate bar determined using equilibrium and compatibility conditions that specify displacement at the supports. Use the load-displacement relationship,  = PL/AE

## Slide 38: CHAPTER REVIEW
Change in temperature can cause member made from homogenous isotropic material to change its length by  = TL . If member is confined, expansion will produce thermal stress in the member
Holes and sharp transitions at x-section create stress concentrations. For design, obtain stress concentration factor K from graph, which is determined empirically. The K value is multiplied by average stress to obtain maximum stress at x-section, max = Kavg

## Slide 39: CHAPTER REVIEW
If loading in bar causes material to yield, then stress distribution that’s produced can be determined from the strain distribution and stress-strain diagram
For perfectly plastic material, yielding causes stress distribution at x-section of hole or transition to even out and become uniform
If member is constrained and external loading causes yielding, then when load is released, it will cause residual stress in the material