## Slide 1: Symmetry Elements II
Notes: <number>

## Slide 2: 3-D Symmetry
We now have 8 unique 3D symmetry operations:
1 2 3 4 6 m 3 4
Combinations of these elements are also possible
A complete analysis of symmetry about a point in space requires that we try all possible combinations of these symmetry elements
Notes: <number>

## Slide 3: Point Group
The set of symmetry operations that leave the appearance of the crystal structure unchanged.
There are 32 possible point groups (i.e., unique combinations of symmetry operations).
Notes: <number>

## Slide 4: 2-D Symmetry
Try combining a 2-fold rotation axis with a mirror
The result is Point Group 2mm
“2mm” indicates 2 mirrors
The mirrors are different
Notes: <number>

## Slide 5: 2-D Symmetry
Now try combining a 4-fold rotation axis with a mirror
Notes: <number>

## Slide 6: 2-D Symmetry
Now try combining a 4-fold rotation axis with a mirror
Step 1: reflect
Notes: <number>

## Slide 7: 2-D Symmetry
Now try combining a 4-fold rotation axis with a mirror
Step 1: reflect
Step 2: rotate 1
Notes: <number>

## Slide 8: 2-D Symmetry
Now try combining a 4-fold rotation axis with a mirror
Step 1: reflect
Step 2: rotate 2
Notes: <number>

## Slide 9: 2-D Symmetry
Now try combining a 4-fold rotation axis with a mirror
Step 1: reflect
Step 2: rotate 3
Notes: <number>

## Slide 10: 2-D Symmetry
Now try combining a 4-fold rotation axis with a mirror
Any other elements?
Notes: <number>

## Slide 11: 2-D Symmetry
Now try combining a 4-fold rotation axis with a mirror
Yes, two more mirrors
Any other elements?
Notes: <number>

## Slide 12: 2-D Symmetry
Now try combining a 4-fold rotation axis with a mirror
Point group name??
Yes, two more mirrors
Any other elements?
Notes: <number>

## Slide 13: 2-D Symmetry
Now try combining a 4-fold rotation axis with a mirror
4mm
Point group name??
Yes, two more mirrors
Any other elements?
Why not 4mmmm?
Notes: <number>

## Slide 14: 2-D Symmetry
3-fold rotation axis with a mirror creates point group 3m
Why not 3mmm?
Notes: <number>

## Slide 15: 2-D Symmetry
6-fold rotation axis with a mirror creates point group 6mm
Notes: <number>

## Slide 16: 2-D Symmetry
The original 6 elements plus the 4 combinations creates 10 possible 2-D Point Groups:
1 2 3 4 6 m 2mm 3m 4mm 6mm
Any 2-D pattern of objects surrounding a point must conform to one of these groups
Notes: <number>

## Slide 17: 3-D Symmetry
As in 2-D, the number of possible combinations is limited only by incompatibility and redundancy
There are only 22 possible unique 3-D combinations, when combined with the 10 original 3-D elements yields the 32 3-D Point Groups
Notes: <number>

## Slide 18: 3-D Symmetry
The 32 3-D Point Groups
  Every 3-D pattern must conform to one of them.
  This includes every crystal, and every point within a crystal
Table 5.1 of Klein (2002) Manual of Mineral Science, John Wiley and Sons
Notes: <number>

## Slide 19: Crystal Systems
A grouping point groups that require a similar arrangement of axes to describe the crystal lattice. |
There are seven unique crystal systems.
Notes: <number>

## Slide 20: 3-D Symmetry
The 32 3-D Point Groups
Regrouped by Crystal System
Table 5.3 of Klein (2002) Manual of Mineral Science, John Wiley and Sons
Notes: <number>

## Slide 21: Triclinic
Three axes of unequal length
Angles between axes are not equal
Point group: 1
Notes: <number>

## Slide 22: Monoclinic
Three axes of unequal length
Angle between two axes is 90°
Point groups: 2, m, 2/m
Notes: <number>

## Slide 23: Orthorhombic
Three axes of unequal length
Angle between all axes is 90°
Point groups: 222 2/m2/m/2/m, 2mm
Notes: <number>

## Slide 24: Tetragonal
Two axes of equal length
Angle between all axes is 90°
Point groups: 4, 4, 4/m, 4mm, 422, 42m, 4/m2/m2/m
Notes: <number>

## Slide 25: Hexagonal
Four axes, three equal axes within one plane
Angle between the 3 co-planar axes is 60°
Angle with remaining axis is 90°
Point groups: 6, 6, 6/m, 6mm, 622, 62m, 6/m2/m2/m
Notes: <number>

## Slide 26: Trigonal (Subset of Hexagonal)
Four axes, three equal axes within one plane
Angle between the 3 co-planar axes is 60°
Angle with remaining axis is 90°
Point groups: 3, 3, 3/m, 32, 32/m
Notes: <number>

## Slide 27: Cubic / Isometric
All axes of equal length
Angle between all axes is 90°
Point groups: 23, 423, 2/m3, 43m, 4/m32/m
Notes: <number>

## Slide 28: Crystal System Characteristics
Isometric/Cubic
Hexagonal
Tetragonal
Orthorhombic
Monoclinic
Triclinic
ALL AXES EQUAL
AXES UNEQUAL
Notes: <number>

## Slide 29: Birefringence
Isometric/Cubic
Hexagonal
Tetragonal
Orthorhombic
Monoclinic
Triclinic
ISOTROPIC
ANISOTROPIC
Notes: <number>

## Slide 30: Crystal System Characteristics
Isometric/Cubic
Hexagonal
Tetragonal
Orthorhombic
Monoclinic
Triclinic
ALL AXES EQUAL
ALL AXES UNEQUAL
TWO AXES EQUAL
Notes: <number>

## Slide 31: Interference Figure
Isometric/Cubic
Hexagonal
Tetragonal
Orthorhombic
Monoclinic
Triclinic
UNIAXIAL
BIAXIAL
Notes: <number>

## Slide 32: Crystal System Characteristics
Isometric/Cubic
Hexagonal
Tetragonal
Orthorhombic
Monoclinic
Triclinic
ALL AXES EQUAL
AXES NON-ORTHOGONAL
AXES ORTHOGONAL
Notes: <number>

## Slide 33: Extinction
Isometric/Cubic
Hexagonal
Tetragonal
Orthorhombic
Monoclinic
Triclinic
PARALLEL
INCLINED
Notes: <number>